## Slide 1: A New Thermal Network Model for GaN HEMTs
Wayne Struble
Oct 18th 2016

## Slide 2: Talk Outline
What is a thermal network model?
Why is a thermal network model so important for GaN HEMTs?
What thermal network models have been used in the past?
Why is this new thermal network model better?
How is the new thermal network model constructed?
  Electrical analog of heat flow equations
  Analytic solution of the heat spreader problem
  Thermal network model implementation into our design tools
Thermal simulations (using new model in ADS) vs measured results
  Simulated junction temperature of 12x173mm GaN on Silicon HEMT vs micro-Raman measurements.
  Thermal transient simulation of 8x125mm GaN on Silicon HEMT vs gate resistance thermometry measurements.
Conclusions

## Slide 3: Thermal Network Model Basics

## Slide 4: What is a Thermal Network Model?
A thermal network model is an electrical equivalent circuit that converts instantaneous dissipated power (heat) in a component (transistor) into an instantaneous temperature. Instantaneous temperature is required as an input for accurate GaN HEMT circuit models.
The thermal network model is an electrical circuit “analog” of the heat flow equations bounded by the physical component’s mechanical construction and thermal properties of the materials used.
Given a thermal heat source (Pdiss), the thermal network response returns voltage (i.e. temperature at the heat source).
Heat Source
Substrate
Die Attach
Package
Baseplate
Temperature
(volts)

## Slide 5: What is a Thermal Network Model? (transistor example)
Below is a example of a transistor with a thermal node, and it’s thermal network model connection (simulating junction temperature).
Thermal
Power is current
Temperature is voltage
Electrical
Pdiss=Vds*Ids (A)
Tbase (V)
Ids
+
Vds
-
Tj (V)
Thermal
Network
Model

## Slide 6: Why is a thermal network model so important for GaN HEMTs?
The electrical properties of GaN HEMTs are “wicked” temperature dependent !!! (EPI sheet Rho, DC IV’s, Gain, Output Power, etc…)
GaN HEMT IV Curves vs Temperature
Mobility & EPI Sheet Rho vs Temperature
typical
operating
range

## Slide 7: What thermal network models have been used in the past?
Simple single-stage fixed RC network.
Drawbacks of this model are:
  No direct physical basis inside the circuit simulator environment.
  Single thermal time constant. (continuum in actual physical structures)
  Values are calculated from measurements or 3D finite element analysis simulations. (i.e. slow) Not calculated inside the circuit simulator.
  Only valid for a fixed geometry, temperature, and dissipated power input.
  Any change in above requires new extracted element values.
Pdiss (A)
Tbase (V)

## Slide 8: What thermal network models have been used in the past?
Multiple-stage fixed RC ladder network. (continuum of time constants)
Drawbacks of this model are:
  Again, no direct physical basis inside the circuit simulator environment.
  Values are calculated from measurements or 3D finite element analysis simulations. (i.e. slow) Not calculated inside the circuit simulator.
  Only valid for a fixed geometry, temperature, and dissipated power input.
  Any change in above requires new extracted element values.
Pdiss (A)
Tbase (V)

## Slide 9: Why is the new thermal network model better?
Benefits of the new model are:
  Has a direct physical basis inside the circuit simulator environment.
  The model is directly calculated using geometry as input, and known material thermal properties over a wide temperature range, so the model very flexible. No model parameter fitting required…
  Speed. The thermal network model temperatures are solved simultaneously within the electrical network it is connected to, so it solves at the same speed as your circuit simulation (i.e. fractions of a second, not minutes).
  Accuracy. Because it is based on known material thermal properties.
  Is valid over a wide range of geometries (substrate thickness, FET fingers, etc.) and temperatures.
  Want to use a different gate pitch, die thickness, unit gate width? No problem, simply change the geometry parameters in the model and re-simulate your circuit to see any performance changes.
  And it’s really cool !!!  (yes, pun intended!)

## Slide 10: Electrical Analog of The Heat Flow Equations
or… How do I solve a physical heat flow problem using a electrical circuit solver?
(i.e. the boring part of the talk!)

## Slide 11: Electrical Analog of the Heat Flow Equations (thermal resistance)
Given a volume of material, the direct heat flow equation is:
q = DT / Rth
where,
q - is the rate of heat conduction (in Watts)
DT – is the temperature difference across the surfaces of a volume (in oC)
Rth – is the thermal resistance of the material (in oC / Watt)
and, Rth = L / (K * A)
L – is the thickness of the material (in cm)
K – is the thermal conductivity of the material (in Watts / (cm-oC) )
A – is the effective area of the material (in cm2)
T1
T2
L
K
A
q
Material Volume

## Slide 12: Electrical Analog of the Heat Flow Equations (thermal resistance)
The “direct current” electrical-thermal analog is now as follows:
I = V / R <=> q = DT / Rth
Current (Amps) represents heat conduction (Watts)
Voltage (Volts) represents temperature (oC)
Resistance (Ohms) represents thermal resistance (oC/Watt)

## Slide 13: Electrical Analog of the Heat Flow Equations (thermal capacitance)
Given a volume of material , the displacement heat flow equation is:
q = Cth dT / dt
where,
q - is the rate of heat conduction (in Watts)
dT / dt – is the rate of change in temperature of the volume (in oC / s)
Cth – is the thermal capacitance (heat capacity) of the material (in Joules / oC)
and, Cth = Cp * m or Cth = Cp * L * A * p
Cp – is the specific heat capacity of the material (in Joules / (Kg-oC) )
m – is the mass of the cell volume (in Kg)
L – is the thickness of the cell (in cm)
A – is the effective area of the cell (in cm2)
p – is the density of the material (in Kg / cm3)
Material Volume
@ Temperature T
L
K
A
q

## Slide 14: Electrical Analog of the Heat Flow Equations (thermal capacitance)
The “displacement current” electrical-thermal analog is now as follows:
i = C dv / dt <=> q = Cth dT / dt
Current (Amps) represents heat conduction (Watts)
Capacitance (Farads) represents heat capacity (Joules / oC)
Rate of change of Voltage (Volts / s) represents rate of change
of temperature (oC / s)
Therefore our electrical “analog” components describing heat flow are shown below: Rth & Cth are nonlinear functions of voltage (temperature)
(Watts)
(oC)
(oC/Watts)
(Joules/oC)
Heat Sources
Fixed Temperatures
Thermal Resistances
Thermal Capacitances

## Slide 15: Analytic solution of the heat spreader problem

## Slide 16: Analytic solution of the heat spreader problem
A well known approximation for solving the heat flow equations (in planar topologies) is to assume that heat flux spreads (from the heat source to the heat sink) at a fixed rate (or angle).
Typically, a 45o spreading angle (or 1:1 spreading factor) is used.
This approximation results in calculated temperatures within 10% of 3D finite element approaches. (for most cases less than a 4% error)
o
heat
source
sink

## Slide 17: Analytic solution of the heat spreader problem (truncated pyramid section)
Below is the analytic solution (for Rth) of this heat spreader problem for a given material. (we sum, i.e. integrate, the DRth versus depth (z) over the thickness of the section, k is assumed constant)
Where area is a function of depth.
T – thickness of the section
SF – spreading factor (45o=1)
x – x dimension of heat source
y – y dimension of heat source

## Slide 18: Analytic solution of the heat spreader problem (truncated pyramid section)
For Cth we assume the specific heat capacity is constant throughout the thin section volume. Then we use the standard equation for Cth.
Cth = Cp * V * p
Cp – is the specific heat capacity of the material (in Joules / (Kg-oC) )
V – is the volume of the section (in cm3)
p – is the density of the material (in Kg / cm3)

## Slide 19: Analytic solution of the heat spreader problem
I now use these analytic solutions for the new thermal network model.
Unfortunately, the material thermal properties are non-linear functions of temperature (i.e. thermal conductivities & specific heat capacities).
Therefore, we have to divide the geometry into thin vertical sections where material thermal properties are assumed constant.
So, the new thermal network model is composed of a cascaded ladder network of RC sections.
Gates
Iso-therms
GaN + AlGaN
Si
Backside of Die

## Slide 20: Analytic solution of the heat spreader problem
Gates
GaN + AlGaN
Si
Backside of Die
Iso-therms
Within each section, we calculate the analytic solution for Rth and Cth using the heat spreader approach.
For GaN on Silicon HEMT’s, the semiconductor is separated vertically into three distinct regions.
  AlGaN+GaN EPI layers (AlGaN+GaN material properties)
  The Silicon substrate under each gate finger before the heat fluxes merge
  The Silicon substrate after the heat fluxes merge (Silicon material properties)
Notes: Spreading factor is a fitting parameter based on measured or simulated thermal behavior

## Slide 21: Thermal network model implementation (multi-finger HEMT concept)
Below I show the
multi-finger heat spreader model
Model Parameters:
GL,UGW, NGF, G2G,
H, SF
All Physical !!!

## Slide 22: Thermal network model implementation into our design tools
Below is the new thermal network model implemented in ADS (we also have this available in AWR)
ADS Model
length of channel heat source
0.4mm for our GaN on Si
technology

## Slide 23: Junction temperature simulation of 12x173mm GaN on Silicon HEMT versus micro-Raman measurements example

## Slide 24: 12x173mm GaN on Silicon HEMT Thermal Simulation
In the following example, I use the new thermal network model to simulate the junction temperature versus dissipated power of a 12x173mm GaN on Silicon HEMT.
The HEMT die is 50mm thick and mounted in a AC360 package using AuSn eutectic die attach (I assumed 12.5mm bond line thickness).
The baseplate temperatures were 25oC and 80oC and dissipated powers simulated/measured were 2-4 Watts/mm (Vds=50v).
Simulated junction temperatures using the new thermal network model are within 4oC of measured mRaman measurements taken at the University of Bristol.

## Slide 25: 12x173mm GaN on Silicon HEMT Thermal Simulation
12x173mm GaN on Si HEMT (50mm thick)
52mm G2G pitch
Thermal Model
HEMT
AC360 package
solder
50mm
12.5mm
1524mm
25,80oC
Pdiss 2-4W/mm
Tj
die

## Slide 26: 12x173mm GaN on Silicon HEMT Thermal Simulation (25oC Baseplate)
New Model Simulation
mRaman Measurements
Micro Raman Measurements
from University of Bristol

## Slide 27: 12x173mm GaN on Silicon HEMT Thermal Simulation (80oC Baseplate)
New Model Simulation
mRaman Measurements
Micro Raman Measurements
from University of Bristol

## Slide 28: Thermal transient simulation of 8x125mm GaN on Silicon HEMT vs gate resistance thermometry measurements example (under pulsed conditions)

## Slide 29: Transient Gate Resistance Thermometry 8x125µm GaN on Si HEMT (Ta=85°C)
The following example demonstrates the new thermal network model under dynamic thermal conditions.

## Slide 30: Transient Gate Resistance Thermometry 8x125µm GaN on Si HEMT (Ta=85°C)
8x125mm GaN on Si HEMT
(50mm thick die 60mm G2G)
GaN on Si Thermal Model
HEMT
copper block
solder
50mm
12.5mm
1600mm
85oC
Pdiss (pulsed)
85oC
GRT measurement
response time
0.2mS
Tj_GRT
Tj
GaN on Si die

## Slide 31: Transient Gate Resistance Thermometry 8x125µm GaN on Si HEMT (Ta=85°C)
GRT Measured Data
Measured Pdiss
GaN on Si Thermal Model
Model Pdiss Input
Gate temperature vs. time and corresponding channel power dissipations

## Slide 32: Summary
I presented a new thermal network model for GaN HEMTs (that is equally adaptable to any other semiconductor technology).
The model is based on fundamental physical and thermal material properties, easy to use, scalable, accurate, fast, and runs within our standard circuit design tools.
I showed two examples using the model that demonstrate accuracy under both static and dynamic thermal environments.
The model is available in our GaN on Silicon design kits for use with the “Jackal” GaN HEMT model in both AWR & ADS.
Thanks for your attention!
Questions?

## Slide 33: Backup Slides

## Slide 34: GaN on Silicon Thermal Network Model
ADS “SDD” Model

## Slide 35: GaN Thermal Cell Model
ADS “SDD” Model

## Slide 36: Silicon Thermal Cell Model
ADS “SDD” Model

## Slide 37: Silicon Thermal Cell Model (fit versus NIST Data)
Thermal Conductivity of Silicon
Specific Heat Capacity of Silicon

## Slide 38: Gold Thermal Cell Model (specific heat capacity only)
ADS “SDD” Model

## Slide 39: Gold Thermal Cell Model (fit versus NIST Data)

## Slide 40: AuSn Solder Thermal Network Model
ADS Model

## Slide 41: AuSn Solder Thermal Cell Model
ADS “SDD” Model
fixed vs temp Kth = 57 W/m-oK
fixed vs temp Cth

## Slide 42: P253 Package Thermal Network Model

## Slide 43: P253 Package Thermal Network Model
ADS Model
Copper
508mm
Moly
508mm
Copper
508mm

## Slide 44: Copper Thermal Cell Model
ADS “SDD” Model

## Slide 45: Copper Thermal Cell Model (fit versus NIST Data)
Thermal Conductivity of Copper
Specific Heat Capacity of Copper

## Slide 46: Moly Thermal Cell Model
ADS “SDD” Model

## Slide 47: Moly Thermal Cell Model (fit versus NIST Data)
Thermal Conductivity of Moly
Specific Heat Capacity of Moly