## Slide 1: WIN NP45-20 GaN on Silicon Jackal Model Oct 4th 2016
Wayne Struble

## Slide 2: Executive Summary
We extracted a Jackal model for the WIN 0.4mm NP45-20 GaN on Silicon process.
The devices tested for model extraction were from wafer WN031P14005.
The devices were tested on a full thickness wafer (625mm).
The devices tested were 2x170mm and 6x170mm CPW FETs.
Both device types have a overlap type source field plate.
The Jackal model was extracted from measured data on the 2x170mm FET and 2.5GHz loadpull was performed on the 6x170mm FET for model verification.

## Slide 3: WIN 0.4mm GaN on Silicon 2x170mm 50v FET Measurement Reference Planes
2x170mm CPW FET
Drain
Gate
Source
Ref Planes
Source

## Slide 4: WIN 0.4mm GaN on Silicon 6x170mm 50v FET Measurement Reference Planes
ADD slide

## Slide 5: Measurement Summary
Below are the measurements that were done for the model extractions.
DC IV characteristics at (-40, 0, 25, 50, 100oC baseplate)
  DC IV’s are out to Vds=30v (Vgs = -4v to +2v, 0.25v steps)
  Forward gate diode current (Vds = 0v, Igs = 1e-5 to 10mA/mm)
  3-terminal gate leakage current (Vgs = -8v, Vds = 0v to 40v, 1v steps)
  Drain current transfer sweep (Vds = 10v, Vgs = -5v to +2v, 0.1v steps)
  We do not measure breakdown voltage (we don’t want to damage the devices that we are modeling). However, Vbr is measured in process ~250-300v and we can use that data for the model (however, this version of the models do not include breakdown).

## Slide 6: Measurement Summary
Pulsed S-params at 2GHz (-40, 0, 25, 50, 100oC baseplate)
  Vdsq=50v, Vgsq=-3v, (Vds=0v to 60v, Vgs = -4v to +1v, 0.25v steps)
  DC Pulse width = 2ms Period = 1000ms, RF pulse IF BW = 5MHz
  We do direct extraction @ 2GHz to fit the nonlinear charges, Gm, Gds, and pulsed drain current IV curve, etc...
CW 0.1-26.5GHz S-parameters at (25oC baseplate)
  (Vds=50v, Ids = 5 to 30mA)
  We use this data to fit the parasitic inductances Lg, Ld, Ls, Tau, Ri…
Gate and Drain lag measurements (-40, 0, 25, 50, 100oC baseplate)
  Gate lag - (Vds=10v fixed, Vgs is pulsed -10v to Ids~20mA/mm)
  Drain lag - (Vgs fixed for Ids~20mA/mm, Vds is pulsed 50v to 10v)
  We use a single step pulse and we capture the drain current response from 20ms to 2s.
  We use this data to extract the gate and drain lag trap models.

## Slide 7: Measurement Summary
In process PCM data (we have this data over temperature as well)
  EPI sheet rho
  Ohmic contact resistance
  Gate metal sheet rho
  We use this data to calculate the access resistances Rg, Rs, & Rd (including their temperature variation).

## Slide 8: Model Verification
We used CW loadpull measurements on a 6x170mm CPW device at 2.5GHz for model verification.
CW loadpull measurements were at 2.5GHz (25oC baseplate)
  Vdsq=50v, Idsq ~ 20mA/mm Pin = small-signal to 3dB compression
  Capture Pin, Pout, Gain, PAE, Ids, Igs

## Slide 9: GaN on Silicon “Jackal” HEMT Model Topology
Gate
Drain
Source
Tj

## Slide 10: GaN on Silicon “Jackal” HEMT Model Topology Gate & Drain Lag Trap Models
Vgs_int
Vgd_int
Tj
Vtrap voltage out

## Slide 11: GaN on Silicon “Jackal” HEMT Model Topology Parasitic Buffer Resistance
Source Ohmic
Drain Ohmic
gate
AlGaN
GaN
Silicon
2-DEG
Parasitic Ga Layer
Source
Drain

## Slide 12: Executive Summary
Jackal model for GaN on Silicon: (coded in Verilog-A)
  supported in both ADS & AWR design software
Model features:
  Model is scalable (unit gate width & number of gate fingers)
  Full nonlinear model (can be run in linear or nonlinear modes)
  Includes thermal node (to connect to a thermal network)
  Includes extra Ids current node (for dynamic loadline analysis)
  Includes gate and drain lag trapping behavior
  Full temperature dependence of nonlinear drain current, gate charge, trap behavior, leakage currents, and access resistances)
  Includes the affect of parasitic buffer resistance (fixed versus temperature for now)
  Breakdown current not included (in this model version)
Thermal network model for GaN on Silicon is included in the kits.

## Slide 13: S-Parameter Fit (Vds=50v Ids=5mA) 2x170mm CPW FET

## Slide 14: S-Parameter Fit (Vds=50v Ids=10mA) 2x170mm CPW FET

## Slide 15: GaN on Silicon “Jackal” Intrinsic HEMT Models
AWR
ADS

## Slide 16: GaN on Silicon “Jackal” Intrinsic HEMT Model
AWR
fixed metal capacitances
gate lag model
drain lag model
Rd model
Rs model
gate Schottky
model
Intrinsic
Jackal
model

## Slide 17: GaN on Silicon “Jackal” Intrinsic HEMT Model
ADS

## Slide 18: Jackal Model Parameter Values (fixed capacitances)
28v Model
50v Model

## Slide 19: Jackal Model Parameter Values (gate schottky diode)
28v Model
50v Model

## Slide 20: Jackal Model Parameter Values (access resistors Rs & Rd)
GaN EPI Sheet Rho 4.32 W/sq / oC

## Slide 21: Jackal Model Parameter Values (access resistors Rs & Rd)
28v Model Rd
50v Model Rd
28v Model Rs
50v Model Rs

## Slide 22: Jackal Model Parameter Values (access resistor Rg)
28v & 50v Models Rg

## Slide 23: Jackal Model Parameter Values (gate and drain lag)
28v & 50v Models Gate Lag
28v & 50v Models Drain Lag

## Slide 24: GaN on Silicon Parasitic Buffer Resistance Model Concept
Source Ohmic
Drain Ohmic
gate
AlGaN
GaN
Silicon
2-DEG
Parasitic Ga Layer

## Slide 25: GaN on Silicon Parasitic Buffer Resistance Models
extrinsic Vs
extrinsic Vd
5.0 for 50v
model
Rbuf varies across wafer
and process. Typical values
range from 1e5 to 2e5 W/sq
(verification used 2e5W/sq)

## Slide 26: Jackal Model Parameter Values (intrinsic HEMT)
28v Model
50v Model

## Slide 27: GaN on Silicon Thermal Resistance Model

## Slide 28: GaN on Silicon Thermal Resistance Model
AWR
ADS

## Slide 29: GaN on Silicon Thermal Resistance Model
ADS “SDD” Model
ADS & AWR Kit Models
Are coded in Verilog-A

## Slide 30: GaN Thermal Cell Model
ADS “SDD” Model
ADS & AWR Kit Models
Are coded in Verilog-A

## Slide 31: Silicon Thermal Cell Model
ADS “SDD” Model
ADS & AWR Kit Models
Are coded in Verilog-A

## Slide 32: Silicon Thermal Cell Model (fit versus NIST Data)
Thermal Conductivity of Silicon
Specific Heat Capacity of Silicon

## Slide 33: Gold Thermal Cell Model (specific heat capacity only)
ADS “SDD” Model
ADS & AWR Kit Models
Are coded in Verilog-A

## Slide 34: Gold Thermal Cell Model (fit versus NIST Data)

## Slide 35: Jackal Model Use (for multi-finger transistor cells)
Must add extrinsic elements
to intrinsic Jackal subcircuit model
Ld
Ls
Lg & Ri
die attach
and package
thermal models
use VCVS so AWR
gets PAE calculation
correct (source power = 0)
Tbase = baseplate temp
i=0
port voltage = Tj
i=Pdiss

## Slide 36: Jackal Model Verification (DC IV’s -40oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT

## Slide 37: Jackal Model Verification (DC IV’s 0oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT

## Slide 38: Jackal Model Verification (DC IV’s 25oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT

## Slide 39: Jackal Model Verification (DC IV’s 50oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT

## Slide 40: Jackal Model Verification (DC IV’s 100oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT

## Slide 41: Jackal Model Verification (S-parameters 25oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT (Vds=30v Ids=20mA)

## Slide 42: Jackal Model Verification (S-parameters 25oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT (Vds=30v Ids=20mA)
S11
S21
S12
S22

## Slide 43: Jackal Model Verification (S-parameters 25oC baseplate) GCS 0.4mm GaN on Silicon 2x200mm 50v HEMT (Vds=50v Ids=20mA)
S11
S21
S12
S22

## Slide 44: 1GHz Pulsed S-param Extract (Vdsq=30v Vgsq=-3v) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT Tbase=25oC
Jackal Model
Measured
pF/mm
mS/mm
Vgs_pulse=-4v to 1v
0.25v steps
Vgs_pulse=-4v to 1v
0.25v steps

## Slide 45: 1GHz Pulsed S-param Extract (Vdsq=30v Vgsq=-3v) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT Tbase=25oC
Measured
pF/mm
mS/mm
Jackal Model
Vgs_pulse=-4v to 1v
0.25v steps
Vgs_pulse=-4v to 1v
0.25v steps

## Slide 46: 1GHz Pulsed S-param Extract (Vdsq=30v Vgsq=-3v) GCS 0.4mm GaN on Silicon 2x200mm 28v HEMT Tbase=25oC
Measured
pF/mm
Jackal Model
Vgs_pulse=-4v to 1v
0.25v steps
Vgs_pulse=-4v to 1v
0.25v steps

## Slide 47: GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT
50v GD5 Device
Drain
Gate
Ref Plane
Ref Plane

## Slide 48: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=30v Ids=20mA)

## Slide 49: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=30v Ids=20mA)
Pout Contours (dBm)
33-36dBm (0.5dB steps)
Pin=22dBm
PAE Contours (dBm)
35-60% (5% steps)
Pin=22dBm

## Slide 50: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=30v Ids=20mA)
Jackal Model
Simulation
Pout=36.4dBm
PAE=61.0%
Gain=14.4dB

## Slide 51: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=30v Ids=20mA)
Measured Data
Pout=36.1dBm
PAE=58.6%
Gain=14.1dB

## Slide 52: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=50v Ids=20mA)

## Slide 53: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=50v Ids=20mA)
Pout Contours (dBm)
32-38dBm (1dB steps)
Pin=23dBm
PAE Contours (dBm)
30-55% (5% steps)
Pin=23dBm

## Slide 54: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=50v Ids=20mA)
Jackal Model
Simulation
Pout=37.7dBm
PAE=60.5%
Gain=14.7dB

## Slide 55: Jackal Model Verification (2.5GHz Loadpull 25oC baseplate) GCS 0.4mm GaN on Silicon 6x167mm 50v HEMT (Vds=50v Ids=20mA)
Measured Data
Pout=37.8dBm
PAE=58.4%
Gain=14.8dB