## Slide 1: MACOM Diode Products rev 0
Joe Bukowski, Rick Cory
31 January 2017

## Slide 2
PRODUCT FAMILIES
Diode Products
PIN/NIP Diodes:
Switching
Attenuation
Limiting
Schottky Diodes:
Detection
Frequency Mixing
Attenuators
Varactor Diodes:
Tuning
Phase Shifting
Passive Devices
RF Chokes/Inductors
MNS Capacitors
Resistors
Multiplier Diodes:
Frequency Multiplication
Waveshaping

## Slide 3
PRODUCT CONFIGURATIONS
Discrete Device
Bare Die
(to 18 GHz)
HMIC Discrete Surmount
(to 26.5GHz)
Beam Lead/ Flip Chip
(to 70+ GHz)
MELF
(to 1 GHz)
Hermetic Packaged
(to 12 GHz)
Plastic
(to 6 GHz)
Integrated Solutions
HMIC, AlGaAs
(to 70+ GHz)
Hybrid Solutions
Multichip Modules
(to 8 GHz)

## Slide 4: PIN Diodes
Switching
Attenuation Receiver Protector Limiting

## Slide 5: PIN Diodes
PIN Diodes used in switches typically have low capacitance and low series resistance
I layer thickness and thermal resistance determine RF power handling
PIN Diodes used in attenuators typically have
  low capacitance for low insertion loss
  thick I layers for large available range of resistance and low distortion
PIN Diodes used in limiters typically have low capacitance for low insertion loss
I layer thickness determines threshold level, recovery time and flat leakage

## Slide 6: PIN Diodes
PIN Diodes are current-controlled RF resistors
Primarily used in control circuits
  Switches
  Attenuators
  (Switched Transmission Line) Phase shifters
MACOM PIN diodes made from Si, GaAs or AlGaAs

## Slide 7: PIN Diode Families
Si Discrete | Si HMIC™ | GaAs | AlGaAs
Wide operating frequency range, to 20 GHz Excellent power handling PIN and NIP diodes available I layer: 2 – 300 µm Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Very Wide operating frequency range, to 30 GHz I layer: 8 – 100 µm Available as Single junction devices Multiple junction ICs Wire-bondable or solderable | Wide operating frequency range, to 30 GHz Good power handling Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Extremely Wide operating frequency range, to 100 GHz Lower insertion loss than comparable Si or GaAs switches I layer: 3 µm Available as Multiple junction ICs Wire-bondable

## Slide 8: PIN Junction
Consists of heavily doped P and N layers separated by undoped Intrinsic layer
Anode
Cathode

## Slide 9: PIN Doping
P layer is heavily doped with acceptor atoms (excess holes) to produce net positive charge
I layer has very light donor doping
N layer is heavily doped with donor atoms (excess electrons) to produce net negative charge
p
n
+++++++++++++++++++++++++++++++++++++++++++++++++++
- - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - -
i
- - - - - - - - - - - - - - - - - - - - - - - - - - -
pn
junction

## Slide 10: Depletion Region
Charge carriers are attracted to each other
At the junction they recombine to form depletion region which has zero net charge
p
n
depletion region
+++++++++++++++++++++++++++++++++++++++++++++++++++
- - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - - -
i
- - - - - - - - - - - - - - - - - - - - - - - - - - -

## Slide 11: Current-Controlled Resistor
Depletion region has zero net charge, which makes it an insulator
P layer is very heavily doped, making it a conductor and source of holes
N layer is very heavily doped, making it a conductor and source of electrons
I layer is very lightly doped, which makes it a resistor with high resistivity

## Slide 12: PIN Junction - Forward Bias
Under forward bias
  Holes are forced from the P layer into the I layer
  Electrons are forced from the N layer into the I layer
Instantaneous population of free holes and electrons in the I layer is increased
Instantaneous resistivity of the I layer is decreased, thereby temporarily decreasing I layer resistance
p
n
+++++++++++++++++++++++++++++++++++++++
- - - - - - - - - - - - - - - - - - - - - - - - - -
i
- + - + - + - + - + - + - + - + - + - + - + -- + - + - + - +
+
-
Current
Source

## Slide 13: I Layer Resistance
RI LAYER = L / A
where
   is the instantaneous resistivity of the I layer
  L is the thickness of the I layer
  A is the area of the I layer
p
n
+++++++++++++++++++++++++++++++++++++++
- - - - - - - - - - - - - - - - - - - - - - - - - -
i
- + - + - + - + - + - + - + - + - + - + - + -- + - + - + - +
+
-
Current
Source

## Slide 14: Resistance versus Bias Current
Small carrier pop.
Increasing carrier population
Saturated carrier population

## Slide 15: I Layer Resistance
RI Layer  kI-
where
  k = series resistance at I = 1 mA
  I is bias current expressed in mA
   is the slope exponent of the RS vs. I curve
Describes the straight-line portion of the curve only

## Slide 16: Simplified PIN Die Equivalent Circuit
LS is series inductance of die (typically 0.15 nH)
Cj is junction capacitance
RI Layer is I layer resistance
RSAT is bulk resistance of P, I and N layers
RP is parallel resistance of I layer

## Slide 17: Packaged PIN Equivalent Circuit
LS is series inductance of die & package (typically 0.4 to 2 nH)
Cpkg is package capacitance (typically 0.13 to 1 pF)
Other components are discussed in die equivalent circuit

## Slide 18: Minority Carrier Lifetime
Minority carrier lifetime is defined as the mean time that a charge carrier exists in the diode before recombination occurs
Symbols for Minority carrier lifetime
  TL
  
Forward Bias
Reverse Bias
TL

## Slide 19: Minority Carrier Lifetime - So What?
If the period of an RF signal is LESS than  AND the magnitude of the RF signal is relatively small, the PIN diode acts as a very linear resistor
The net amount of charge in the I layer is a primary determinant of the resistance produced by the diode
The net amount of charge in the I layer can be controlled by a low frequency (DC) bias current
BUT
If the period of an RF signal is GREATER than  OR the magnitude of the RF signal is very large, the diode rectifies

## Slide 20: PIN Diode Applications
Switch
Attenuator
Power Limiter

## Slide 21: PIN Diode Switch
The impedance of an ideal switch has two states
  short (0 )
  open ( )
A PIN diode comes very close - resistance can vary more than 4 orders of magnitude
Almost an open
Almost a short

## Slide 22: Desirable Properties - Switch PINs
Low capacitance
Wide range of resistance
Low minority carrier lifetime for fast switching
Sufficiently large breakdown voltage to handle RF signal and bias voltages
Small dC/dV for low distortion

## Slide 23: PIN Switch Topologies
Two fundamental configurations
  Series diode
  Shunt diode
All other switch configurations are combination of series and shunt
Switches are reflective
Series
Switch
Shunt
Switch

## Slide 24: Series Switch
Isolation determined by capacitive reactance
  Function of frequency
Insertion loss determined by resistance
  Independent of frequency
Series
Switch

## Slide 25: Shunt Switch
Insertion loss isolation determined by capacitive reactance
  Function of frequency
Isolation determined by resistance
  Independent of frequency
Shunt
Switch

## Slide 26: Series-Shunt Switch
Insertion loss and isolation determined by series and shunt diode combination
Insertion loss and isolation are functions of
  signal frequency
  diode resistance
Series-Shunt

## Slide 27: PIN Diode Attenuator
The ideal attenuator element requires a continuously-variable impedance
A PIN diode has continuously-variable impedance between Rp and RSAT
Low Z
High Z
Continuously Variable Z

## Slide 28: Desirable Properties - Attenuator PIN
Low capacitance
Wide range of resistance
Very predictable RS vs. IBIAS curve
Large minority carrier lifetime for low distortion
Small dC/dV for low distortion

## Slide 29: Attenuator Topologies
Reflective
  Single series or shunt diode
  Reflects portion of input signal by creating impedance mismatch
Absorptive
  Dissipates portion of input signal heat
  Several topologies
    
    Tee
    Bridged tee
    Hybrid coupler
      Series
      Shunt

## Slide 30: Series Attenuator
Reflective
Requires diode with very large RS at low IBIAS
Requires diode with very small Ct
Series
Attenuator

## Slide 31: Shunt Attenuator
Reflective
Reasonable attenuation versus IBIAS curve
Shunt
Attenuator

## Slide 32:  Attenuator
Matched (Absorptive)
The RS vs. IBIAS of the shunt diodes must be identical
The RS vs. IBIAS of the shunt and series diodes must be “complementary” to maintain the desired input and output impedances

## Slide 33:  Attenuator Resistance vs. Attenuation

## Slide 34: Tee Attenuator
Matched (Absorptive)
The RS vs. IBIAS of the series diodes must be identical
The RS vs. IBIAS of the shunt and series diodes must be “complementary” in order to maintain the desired input and output impedances

## Slide 35: Tee Attenuator Resistance vs. Attenuation

## Slide 36: Bridged Tee Attenuator
Matched (Absorptive)
The RS vs. IBIAS of the shunt and series diodes must be “complementary” to maintain the desired input and output impedances
Only 2 diodes & 2 resistors required
Z0
Z0

## Slide 37: Bridged Tee Attenuator Resistance vs. Attenuation

## Slide 38: Hybrid Coupler Attenuator - Series Diodes
Absorptive
Requires hybrid coupler, two diodes, two resistors and capacitors
RS vs. IBIAS for diodes must be matched
Input
Output
Zo
Zo

## Slide 39: Hybrid Coupler Attenuator - Series Diodes R vs. Attenuation

## Slide 40: HIP3™ Variable Attenuators

## Slide 41: Hybrid Coupler Attenuator - Shunt Diodes
Absorptive
Requires coupler, two diodes, two resistors and capacitors
RS vs. IBIAS for diodes must be matched
Input
Output
Zo
Zo

## Slide 42: Hybrid Coupler Attenuator - Shunt Diodes R vs. Attenuation

## Slide 43: PIN Diode Limiters
Limiters are used to protect sensitive, delicate circuits such as low noise amplifiers and mixers from large input signals
PIN diode acts as an input-power-controlled variable resistance
Resistance is inversely proportional to incident power
As input power increases, so does impedance mismatch and transmission loss

## Slide 44: Incident Power Controlled Variable Attenuator

## Slide 45: Discrete Diodes – Limiters
Limiter diodes available
  Die Versions (to 20 GHz)
  Available in Ceramic & Plastic Packages (up to 12 GHz)
  Low Capacitance
  I layers from 2 µm to 40 µm
  Cascadable for Increased Power Handling and Limiting
    Thinnest diode placed at output stage
      Determines threshold level, spike leakage
    Thickest diode placed at input stage
      Determines power handling, recovery time
/4
I standing wave
V standing wave
Thin “clean-up” limiter
Thick “coarse” limiter

## Slide 46: Output Waveform of Limiter
Transmitted Power
Time (µs)
T spike
Spike Peak Power
Flat Leakage
Recovery

## Slide 47: Limiter Recovery Waveform
Transmitted Power
Time ( s )
3 dB point
for signal voltage
100 % Low Power Recovery Ref Signal
RF High Power Pulse

## Slide 48: Summary
PIN diodes are low-frequency-current-controlled RF/microwave resistors
PIN diodes are used in switches, attenuators and power limiters
MACOM PIN diodes are made from Si, GaAs or AlGaAs

## Slide 49: Thank You

## Slide 50: Appendix

## Slide 51
RF Power and Frequency Performance vs Diode Type
MELF
CW Incident Power (W)
0.1
1.0
10
100
1k
0.01
0.1
AlN in 3mm, 4mm DFN
Die
3KV Ceramic
SURMOUNT
SOD, SOT, Without AlN
Flip Chip, BL
1.0
10
100
F (GHz)
Best Choice for SMT
Best Choice for Wire Bonding

## Slide 52
Si PIN DIODE SWITCH ELEMENT
Series PIN Diode Element
Shunt PIN Diode Element
Series PIN Diode, Thermal-to-Ground Element
Series-Shunt PIN Diode Element
Series, Shunt or Series-Shunt PIN Diodes
SMT Plastic Package
Medium Power Handling

## Slide 53: Discrete Kilovolt PIN Diodes
Features
High Voltage Handling:
  Up to 2000 V, 3000 V
Power Handling: 1 kW
Operate from LF to 500 MHz
Long Carrier Lifetime: 30 µs, 65 µs
Very Low Thermal Resistance:
3 C/W, 4 C/W
Very Low Resistance: 0.1 Ω, 0.15 Ω
Applications
High Power and High Voltage Switching
Plasma Etching Systems
HF Radio Antenna Tuners

## Slide 54: Discrete High Power MELF PIN Diodes
Available in Tape & Reel
Features
High Voltage Handling: Up to 1100 V
200+ W Power Handling
Operate/Tunable from LF to 2.5 GHz
Surface Mountable
Non-Magnetic Versions
Superior Heat Management
Low Series Resistance
Applications
High Power Switches
Attenuators
Magnetic Resonance Imaging (MRI) Receiver Protection
#1 Supplier of MELF PIN Diodes
Notes: February 16, 2017

## Slide 55
Discrete Limiter Products
Schottky-Limiter-PIN Shunt Antiparallel Pair
Shunt Limiter PIN
Limiter PIN
Broadband Performance to 12 GHz and Higher
Several Packages Available Including
  Low Inductance Shunt Configuration Plastic 1.5 X 1.2 mm DFN
  Ceramic
  Chips
Cascadable

## Slide 56: PIN Switches
Modules Single-Chip

## Slide 57: AlGaAs PIN Diode Switches
SP5T
Product Offering
  SPST to SP8T
Features
  Operating Frequency = 50 MHz - 70 GHz
  Maximum RF Average Incident Power = 0.25 W CW
  AlGaAs ~ 0.3 dB Lower IL (20 GHz) vs. GaAs & Si Switches
  Very Low Insertion Loss
  Excellent Isolation
  Low Switching Time
SPST
SP2T

## Slide 58: AlGaAs SP3T W Band Switch MASW-011029
Broadband Operating Frequency: 60 - 110 GHz
Insertion Loss:1.3 dB Typical
Isolation: 33 dB Typical
Silicon Nitride Passivation
BCB Scratch Protection
Collision Avoidance Radar
Passive Imaging

## Slide 59: Multichip Module High Power Switches
Input power handling to 200 W CW, 1 kW peak
Frequency Range: 20 MHz – 6 GHz in three bands
Symmetric and Asymmetric Designs
SP2T, SP3T, SP4T, SP6T

## Slide 60: T/R Switch-Limiter Module MSWLM2420-242
Features
Frequency Range: 2 – 4 GHz
  T/R switch with passive receiver protection detector/limiter
    Excellent Rx path insertion loss with 2 W CW receiver protector limiter stage
TX input power: 125 W CW, 200 W pk
  Packaged in 5 x 8 mm, low-thermal-resistance surface-mount module package
  Proven performance in the field
Applications
Phased array radar T/R modules
Radio transceiver

## Slide 61: MASW-011036 Ka-Band High Power Terminated AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss <1 dB; High Isolation >38 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
23 dBm power handling in terminated port
Notes: Delete specs table?

## Slide 62: MASW-010646 Ka-Band High Power Reflective AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss: 0.6 dB
High Isolation: 32 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
Notes: Delete specs table?

## Slide 63: X-Band Terminated SPDT Switch MASW-011071
Low Insertion Loss: 1 dB
High Isolation: 38 dB
Integrated Bias Network and Termination Circuit
Greater than 20 W CW Power Handling @ 70 °C
Lead (Pb)-Free 7 x 7 mm 44-lead PQFN Package
Missile Defense, Weather Radar Systems

## Slide 64: HMIC Si PIN Switches: 2 W, DC – 26 GHz
Products
  MASW-001100-11900W (SPST)
  MASW002100-11910W (SPDT)
  MASW-003100-19220W (SP3T)
  MASW-004100-11930W (SP4T)
  MASW-005100-11940W (SP5T)
Features
  Operating Frequency
    50 MHz – 30 GHz
  Series-Shunt Configuration
  High Isolation: >35 dB
  Low Loss: <1.0 dB Insertion Loss
  Switching Time: 50 ns
  Max RF Incident Power:
    >6.0 W CW @ 2 GHz
    2.0 W CW @ 22 GHz
  RoHS Compliant
SP5T
SP3T w/ Integrated Bias Network
Notes: 64

## Slide 65: HMICTM Wire-Bondable Switches
Features
SPST through SP6T
Broadband Performance to 26 GHz
Wire /Ribbon Bond Connections
Available With or Without Integrated Bias Networks
SP3T with Bias Network
SP5T without Bias Network

## Slide 66: HMICTM SP2T High Current MASW-011052
Broad Bandwidth: Specified up to 18 GHz, Usable up to 26 GHz
Integrated Bias Network: High Bias Current +/- 60 mA
Low Insertion Loss/High Isolation
Glass Encapsulation Construction
RoHS Compliant and 260 °C Reflow Compatible

## Slide 67: HMICTM SP3T High Current MASW-011053
Broad Bandwidth: Specified up to 18 GHz, Usable up to 26 GHz
Integrated Bias Network: High Bias Current +/- 60 mA
Low Insertion Loss/High Isolation
Glass Encapsulation Construction
RoHS Compliant and 260 °C Reflow Compatible

## Slide 68: Limiter Modules

## Slide 69: High Power Limiter Modules
Industry-leading input power handling as high as
  300 W CW
  2 kW peak
No external control signal or bias required
Available as
  Single stage
  Dual stage
  Detector/limiter
Available in VHF, UHF, L, S and C bands
Packaged in low-thermal-resistance surface-mount hermetic or nonhermetic module packages

## Slide 70: Discrete Diodes – Si PIN Chips
High Voltage Handling: up to 1000 V
Power Handling: 200+ Watts
Operate from LF to 18 GHz
Chip and Wire Assembly
Low Series Resistance
Applications: Switching and Attenuating
Part Number | Breakdown Voltage (V) | Capacitance (pF) | Series Resistance () | Carrier Lifetime (s) | Thermal Resistance (ºC/W) | I-region (m)
MADP-000165-01340W | 200 | 0.06 | 2.50 | 0.20 | 150 | 19
MA4P161-134 | 100 | 0.10 | 1.50 | 0.150 | 65 | 13
MA47416-132 | 200 | 0.15 | 6.00 | 2.00 | 30.0 | 110
MA47418-134 | 200 | 0.15 | 3.00 | 1.00 | 25.0 | 48
MA4P203-134 | 100 | 0.15 | 1.50 | 0.150 | 75.0 | 13
MA4P303-134 | 200 | 0.15 | 1.50 | 0.20 | 85 | 19
MA4P404-132 | 250 | 0.20 | 0.70 | 0.60 | 30.0 | 28
MA4P504-132 | 500 | 0.20 | 0.60 | 1.00 | 35.0 | 44
MA4P604-131 | 1000 | 0.30 | 1.00 | 3.00 | 10.0 | 96
MA4P505-131 | 500 | 0.35 | 0.45 | 2.00 | 14.0 | 96
MA4P606-131 | 1000 | 0.60 | 0.70 | 4.00 | 8.0 | 96
MA4P506-131 | 500 | 0.70 | 0.30 | 3.00 | 11.0 | 51
MA4P607-212 | 1000 | 1.30 | 0.40 | 5.00 | 4.0 | 125
Notes: February 16, 2017

## Slide 71: Discrete Diodes – Si NIP Chips
High Voltage Handling: up to 500 V
Power Handling: 50+ Watts
Operate from LF to 12+ GHz
Chip and Wire Assembly or Available in Packages
Low Series Resistance
Applications: Switching and Attenuating
Notes: February 16, 2017

## Slide 72: Si Mesa Beamlead PIN Diodes
Rugged Silicon-Glass Construction
Silicon Nitride Passivation
Low Parasitic Capacitance and Inductance

## Slide 73: Si Planar Beamlead PIN Diodes
Rugged Silicon-Glass Construction
Silicon Nitride Passivation
Low Parasitic Capacitance and Inductance

## Slide 74: Flip Chip Products
PIN Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct Max | Rs Typical | Material
 |  | (GHz) | (V) | (pf) | () | 
MA4GP907 | Single | 40 | 45 | 0.025 | 4.2 | GaAs
MA4AGP907 | Single | 50 | 50 | 0.020 | 4.2 | AlGaAs
MA4FCP200 | Single | 40 | 50 | 0.015 | 2.8 | HMIC
MA4FCP300 | Single | 30 | 70 | 0.025 | 2.6 | HMIC
MA4FCP305 | Single | 18 | 40 | 0.050 | 2.1 | HMIC
Varactor Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct 4V | Gamma | Material
 |  | (GHz) | (V) | (pf) |  | 
MA46H146 | Single | 60 | 26 | 0.033-0.06 | 1 | GaAs
MA46H120 | Single | 60 | 15 | 0.20-0.40 | 0.5 | GaAs
Low Capacitance Devices

## Slide 75: Discrete High Power MELF PIN Diodes
Available in Tape & Reel
High Voltage Handling: Up to 1100 V
200+ W Power Handling
Operate/Tunable from DC to 2.5 GHz
Surface Mountable
Non-Magnetic Versions
Superior Heat Management
Low Series Resistance
Applications
High Power Switches
Attenuators
Magnetic Resonance Imaging (MRI)
Part Number | Breakdown Voltage | Total Capacitance | Series Resistance | Carrier Lifetime | Thermal Resistance 
 | (V) | (pF) | () | (s) | (ºC/W)
MA4P504-1072T | 500 | 0.5 | 0.6 | 1.0 | 15
MA4PH236-1072T | 200 | 0.5 | 3.00 | 1.5 | 25
MA4PH238-1072T | 200 | 0.5 | 6.00 | 2.0 | 25
MA4P404-1072T | 250 | 0.6 | 0.60 | 0.6 | 10
MA4P505-1072T | 500 | 0.7 | 0.45 | 2.0 | 6
MA4P7006F-1072T | 600 | 0.7 | 0.90 | 3.0 | 50
MA4P7417-1072T | 800 | 0.7 | 0.80 | 6.5 | 13
MA4P7104F-1072T | 400 | 1.0 | 0.50 | 2.5 | 50
MA4P506-1072T | 500 | 1.0 | 0.30 | 3.0 | 10
MA4P1250-1072T | 50 | 1.2 | 0.75 | 2.0 | 15
MA4PH235-1072T | 35 | 1.2 | 0.50 | 0.3 | 20
MADP-000234-10720T | 500 | 1.7 | 0.25 | 1.5 | 30
MA4P4301F-1091T | 100 | 2.0 | 1.00 | 8.0 | 30
MA4P4306F-1091T | 600 | 2.0 | 1.00 | 8.0 | 30
MA4P4006F-1091T | 600 | 2.2 | 0.50 | 6.0 | 20
MA4P1450-1091T | 50 | 2.5 | 0.75 | 2.0 | 5
MA4P7418-1072T | 1100 | 0.8 | 1.20 | 5.0 | 13
Non Magnetic Package | MA4P7441F-1091T | 100 | 2.2 | 0.50 | 18 | 5
 | MA4P7446F-1091T | 600 | 2.2 | 0.50 | 18 | 6
 | MA4P7452F-1072T | 150 | 0.7 | 0.90 | 9 | 15
 | MA4P7461F-1072T | 100 | 1.0 | 0.50 | 6 | 15
 | MA4P7464F-1072T | 400 | 0.8 | 0.60 | 4.5 | 20
 | MA4P7470F-1072T | 800 | 0.7 | 0.80 | 6.5 | 13
 | MADP-000235-10720T | 35 | 1.2 | 0.50 | 0.3 | 20
#1 Supplier of MELF PIN DIODES
Notes: February 16, 2017

## Slide 76: PIN DIODE SWITCH ELEMENT
Discrete Series PIN Diode
Plastic Package
Medium Power Handling
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MSWSE-005-10S | 5 | 6 | 0.15 | 0.2 | 0.25 | 26 | 17 | 10 | 402
MSWSE-005-15 | 4 | 6 | 0.2 | 0.25 | 0.45 | 24 | 17 | 10 | 503
MSWSE-010-15 | 10 | 2.5 | 0.25 | 0.25 | – | 18 | 9 | – | 503
MSWSE-010-15S | 10 | 3 | 0.05 | 0.25 | – | 20 | 15 | – | 0402P
MSWSE-010-16S | 10 | 3 | 0.06 | 0.08 | – | 20 | 14 | – | 0402P
MSWSE-020-05 | 20 | 1 | 0.05 | – | – | 8 | – | – | 503
MADP-010630-13920T | 25 | 3 | 0.15 | 0.35 | - | 17 | 9 | - | 0805
MSWSE-020-10 | 20 | 1 | 0.03 | – | – | 18 | – | – | 503
MADP-010631-13920T | 40 | 1 | 0.05 | 0.08 | - | 7 | - | - | 0805
MSWSE-040-10 | 40 | 3 | 0.1 | 0.2 | – | 20 | 12 | – | 0805P
MSWSE-044-10 | 40 | 2 | 0.15 | 0.3 | – | 15 | 8 | – | 0805P
MSWSE-050-10 | 50 | 1 | 0.1 | – | – | 10 | – | – | 0805P
MADP-010633-13920T | >50 | 3 | 0.15 | 0.30 | - | 15 | 7 | - | 0805
MSWSE-050-17 | 40 | 3 | 0.06 | 0.1 | – | 18 | 11 | – | 0805P
MSWSER-070-10 | 80 | 0.8 | 0.06 | – | – | 10 | – | – | 3023
MSWSER-100-05 | 80 | 0.8 | 0.15 | – | – | 10 | – | – | 3023
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package*
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MEST2G-010-20 | 10 | 10 | 0.3 | 0.3 | 0.45 | 31 | 23 | 18 | 2012
MEST2G-020-15 | 20 | 6 | 0.2 | 0.22 | 0.3 | 25 | 20 | 11 | 2012
MEST2G-050-45 | 50 | 2.5 | 0.15 | 0.15 | – | 16 | 10 | – | 2615
MEST2G-050-80 | 50 | 1.5 | 0.15 | 0.2 | – | 14 | 8 | – | 2615
MEST2G-010-20 | 10 | 10 | 0.3 | 0.3 | 0.45 | 31 | 23 | 18 | 2012

## Slide 77: PIN DIODE SWITCH ELEMENT
Part Number | Rated CW Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package*
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MEST2G-025-10 | 25 | 4 | 0.06 | 0.3 | - | 18 | 12 | - | CM32
MEST2G-080-25 | 80 | 10 | 0.2 | 0.25 | 0.45 | 30 | 24 | 17 | CM27
MEST2G-100-20-CM33 | 100 | 2.6 | 0.15 | 0.2 | – | 16.5 | 10 | – | CM33
MEST2G-150-10-CM30 | 15W | 1 | 0.07 | - | - | 6 | - | - | CM30
MEST2G-150-10-CM32 | 150 | 2 | 0.12 | 0.16 | - | 12 | 6 | - | CM32
MEST2G-160-10-CM33 | 160 | 2.8 | 0.06 | 0.6 | - | 28 | 20 | - | CM33
MADP-011037 | >125 | 3 | 0.1 | 0.3 | - | 16 | 8 |  | 3mm QFN
Die mounted on thermally-conductive, electrically-insulating substrate
  Very low thermal resistance for high-power handling
CMxx Packages:
QFN Package:

## Slide 78: Shunt PIN Element
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MSWSH-020-24 | 25 | 26 | 0.05 | 0.2 | 0.3 | 28 | 27 | 26 | 2020
MSWSH-020-30 | 20 | 6 | 0.05 | 0.15 | 0.35 | 35 | 31 | 26 | 2012
MSHSH-040-30 | 40 | 6 | 0.04 | 0.1 | 0.3 | 35 | 32 | 36 | 2012
MSWSHC-040-40 | 40 | 10 | 0.1 | 0.2 | 0.4 | 35 | 55 | 50 | 2615
MSWSHB-020-30 | 40 | 10 | 0.02 | 0.08 | 0.13 | 40 | 40 | 35 | 2012
Plastic Over-Mold Package
Very Low Inductance Package for High Isolation

## Slide 79: HMICTM Discrete Diode Solution
Part Number | Size (mils) | VB (V) | 1 MHz | 100 MHz |  |  | 1 GHz |  |  |  |  | Lifetime (ns) | Nominal I-region (m)
 |  |  | Cj 40 V (pF) | Rs 10 mA () | Rs 20 mA () | Rs 100 mA () | Cj 40 V (pF) | Rs 10 mA () | Rs 20 mA () | Rs 50 mA () | Rs 70 mA () |  | 
MADP-042305 | 22 X 41 | 80 | 0.13 |  |  |  | 0.14 |  | 1.32 | 1.18 |  | 180 | 7
MADP-042405 | 22 X 41 | 80 | 0.57 |  |  |  | 0.58 |  | 0.62 | 0.58 |  | 255 | 7
MADP-042505 | 22 X 41 | 80 | 0.27 |  |  |  | 0.27 |  | 0.83 | 0.76 |  | 210 | 7
MADP-042905 | 22 X 41 | 80 | 0.06 |  |  |  | 0.06 |  | 3.14 | 2.6 |  | 140 | 7
MA4SPS302 | 23 X 55 | 70 | 0.40 | 1 |  |  | 0.30 | 1.3 |  |  |  | 460 | 10
MA4SPS402 | 20 X 49 | 70 | 0.034 | 4.6 |  |  | 0.04 | 5 |  |  |  | 200 | 10
MADP-017015-1314 | 60 X 30 | 115 | 0.32 |  |  |  | 0.31 | 0.72 |  |  | 0.51 | 1300 | 15
MADP-030015-1314 | 60 X 30 | 115 | 0.79 |  |  |  | 0.78 | 0.49 |  |  | 0.38 | 1600 | 15
MADP-017025-1314 | 60 X 30 | 135 | 0.23 |  |  |  | 0.23 | 1.01 |  |  | 0.64 | 2300 | 25
MADP-030025-1314 | 60 X 30 | 135 | 0.50 |  |  |  | 0.50 | 0.65 |  |  | 0.45 | 2800 | 25
MA4SPS502 | 23 X 57 | 200 | 0.14 |  | 2.4 | 1.4 | 0.09 |  |  |  |  | 2800 | 50
MA4SPS552 | 12 X 22 | 200 | 0.08 |  | 2.4 | 1.7 | 0.06 |  |  |  |  | 2500 | 50
MA4SPS421 | 20 X 41 | 200 | 0.09 |  |  |  | 0.07 | 6.2 |  |  |  | 5000 | 100
MA4SPS422 | 20 X 41 | 200 | 0.18 |  |  |  | 0.13 | 3.1 |  |  |  | 10000 | 100
MADP-042308-1306 | 20 X 41 | 100 | 0.20 |  |  |  | 0.10 |  | 1.38 | 1.18 |  | 280 | 10
MADP-042408-1306 | 20 X 41 | 100 | 0.50 |  |  |  | 0.37 |  | 0.67 | 0.61 |  | 380 | 10
MADP-042508-1306 | 20 X 41 | 100 | 0.30 |  |  |  | 0.18 |  | 0.97 | 0.87 |  | 310 | 10
MADP-042908-1306 | 20 X 41 | 100 | 0.15 |  |  |  | 0.05 |  | 3.63 | 3.02 |  | 230 | 10
Surmount PIN diodes
Available I-region Thickness: 7 to 100 µm

## Slide 80: Discrete Diodes – Limiters
Die Versions (to 20 GHz)
  Available in Ceramic & Plastic Packages (up to 12 GHz)
  Low Capacitance
  Cascadable for Increased Power Handling and Limiting
  Au-doped and non-Au-doped diodes available to optimize recovery time and flat leakage power
Part Number | Min VB | Max VB | Min Cj @ 0 V | Max Cj @ 0 V | Max Rs @ 10 mA | Nominal Characteristics |  |  | 
 |  |  |  |  |  | Carrier Lifetime | Intrinsic Region Thickness | Contact Diameter | Thermal Resistance
 | V | V | pF | pF |  | ns | m | mils | ºC/W
MA4L011-134 | 15 | 35 | 0.08 | 0.18 | 2.10 | 10 | 2 | 1.2 | 175
MA4L021-134 | 20 | 35 | 0.10 | 0.20 | 2.10 | 10 | 2 | 1.2 | 175
MA4L022-134 | 20 | 35 | 0.09 | 0.19 | 2.00 | 10 | 2 | 1.2 | 175
MADL-011009-0134 | 20 | 35 | 0.16 | 0.23 | 1.50 | 10 | 2 | 3.0 | 175
MA4L031-134 | 30 | 50 | 0.14 | 0.21 | 2.00 | 20 | 3 | 1.4 | 150
MA4L032-134 | 30 | 50 | 0.13 | 0.20 | 2.50 | 15 | 3 | 1.5 | 150
MADL-011010-0134 | 30 | 50 | 0.17 | 0.24 | 1.50 | 15 | 3 | 3.0 | 150
MA4L062-134 | 60 | 75 | 0.07 | 0.15 | 2.50 | 10 | 4 | 1.5 | 150
MADL-011011-0134 | 60 | 75 | 0.05 | 0.17 | 2.30 | 10 | 4 | 3.0 | 150
MA4L101-134 | 100 |  |  | 0.15 | 2.00 | 90 | 13 | 3.5 | 30
MADL-000301-0134 | 200 |  |  | 0.20 | 1.50 | 200 | 20 | 3.0 | 30
MA4L401-134 | 250 |  |  | 0.30 | 1.20 | 800 | 25 | 4.5 | 25

## Slide 81: HMIC and AlGaAs MMIC Performance Comparison
Parameter | HMIC | AlGaAs
Products | Switches, Attenuators, Limiters | Switches
Medium | Silicon and Glass | Semi-Insulating GaAs
Die Thickness (um) | 125 | 100
Intrinsic Length (um) | 8 to 100 | 3
I/O Connections | Wire Bondable and SMT | Wire Bondable Only
Passive R,L,C Integration | Yes | Yes
Breakdown Voltage (V) | 50 to 200 | 70
F (GHz) | 0.050 - 30 | 0.050 - 70
Insertion Loss at 10 GHz (SP4T) | 0.6 | 0.45
Switching Speed (ns) | 100 | 15
IIP3 (dBm) | 45 | 25
CW Power Handling, @ 2 GHz (dBm) | +38 | +23

## Slide 82: AlGaAs Products
Topology | Frequency (GHz) | Insertion Loss (dB) | Isolation (dB) | P1dB (dBm) | Reflective or Absorptive | Bias (mA) | Part Number | Package
SPST | 0.05 - 18 18 – 50 | 0.2 0.3 | 22 46 | 23 | Reflective | 10 | MA4AGSW1 | DIE
SPST | 10-50 | 1.2 | 30 | 23 | Absorptive | 10 | MA4AGSW1A | DIE
SP2T | 0.05 - 18 18 – 50 | 0.5 0.7 | 47 33 | 23 | Reflective | 10 | MA4AGSW2 | DIE
SP3T | 0.05 - 18 18 – 50 | 0.6 0.8 | 45 31 | 23 | Reflective | 10 | MA4AGSW3 | DIE
SP4T | 0.05 - 18 18 – 50 | 0.7 1.0 | 41 32 | 23 | Reflective | 10 | MA4AGSW4 | DIE
SP5T | 0.05 - 18 18 – 50 | 1.4 1.9 | 35 30 | 23 | Reflective | 10 | MA4AGSW5 | DIE
SP8T | 0.05 - 18 18 - 50 | 1.5 2.0 | 32 32 | 23 | Reflective | 10 | MA4AGSW8-1 | DIE

## Slide 83: MASW-011036 Ka-Band High Power Terminated AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss <1 dB; High Isolation >38 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
23 dBm power handling in terminated port
Notes: Delete specs table?

## Slide 84: MASW-010646 Ka-Band High Power Reflective AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss: 0.6 dB
High Isolation: 32 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
Notes: Delete specs table?

## Slide 85: HMICTM SP2T 6-14 GHz (Terminated SPDT) MASW-010647
X-Band Terminated SPDT switch
Wire-Bondable Bare Die
Low Insertion Loss/ High Isolation
All Shunt Design; Integrated Bias Network
Glass Encapsulated Construction
Greater than 20 W CW Power Handling @ 85 °C
Silicon Nitride Passivation/Polymer Scratch Protection
RoHS Compliant
Notes: Delete specs table?

## Slide 86: HMICTM Package-less Surface Mountable Si PIN Diode Switches
Topology | Frequency | Insertion Loss (dB) | Isolation (dB) | P0.1dB (dBm) | Part Number
SPDT | 6 GHz 13 GHz 20 GHz | 0.6 0.9 1.2 | 45 31 25 | 36 | MASW-002103-1363
SP3T | 6 GHz 13 GHz 20 GHz | 0.65 0.95 1.25 | 37 28 22 | 36 | MASW-003103-1364
SP4T | 6 GHz 13 GHz 20 GHz | 0.7 1.0 1.3 | 35 30 26 | 36 | MASW-004103-1365
Surface mount - No wirebonds
Packageless - Low parasitics
Series/Shunt multi-throw designs
High Power - 6 W incident

## Slide 87: HMIC™ Si PIN SP2T 6-14 GHz MASW-011021
Specified from 8 GHz to 12 GHz ; Usable 6-14 GHz
Low Insertion Loss / High Isolation
All Shunt Design; Integrated Bias Network
Surface Mountable, Fully Monolithic Die
Glass Encapsulated Construction
20 W Pulsed Power Handling
Silicon Nitride Passivation / Polymer Scratch Protection
RoHS Compliant
Notes: Delete Specs Table?