## Slide 1: MACOM Diode Products rev 7
Joe Bukowski, Rick Cory
1 August 2016

## Slide 2: Diode Products Training
Week 1 - General MACOM diode overview
Week 2 - PIN Diode and Limiter theory/application/products.
Week 3 - Schottky Diode and Limiter theory, applications & products.
Week 4 - The HMIC process, including process overview, products, and performance benefits.
Week 5 - The AlGaAs process, including process overview, products, and performance benefits.
Week 6 - MACOM’s diode/switch product roadmaps
Week 7 - Comb Generators including theory, products in development, and application.

## Slide 3
PRODUCT FAMILIES
Diode Products
PIN/NIP Diodes:
Switching
Attenuation
Limiting
Schottky Diodes:
Detection
Frequency Mixing
Attenuators
Varactor Diodes:
Tuning
Phase Shifting
Passive Devices
RF Chokes/Inductors
MNS Capacitors
Resistors
Multiplier Diodes:
Frequency Multiplication
Waveshaping

## Slide 4
PRODUCT CONFIGURATIONS
Discrete Device
Bare Die
(to 18 GHz)
HMIC Discrete Surmount
(to 26.5GHz)
Beam Lead/ Flip Chip
(to 70+ GHz)
MELF
(to 1 GHz)
Hermetic Packaged
(to 12 GHz)
Plastic
(to 6 GHz)
Integrated Solutions
HMIC, AlGaAs
(to 70+ GHz)
Hybrid Solutions
Multichip Modules
(to 8 GHz)

## Slide 5
DIODES & PASSIVE DEVICES
Diode Products
PIN/NIP Diodes:
Switching
Attenuation
Limiting
Schottky Diodes:
Detection
Frequency Mixing
Attenuators
Varactor Diodes:
Tuning
Phase Shifting
Passive Devices
RF Chokes/Inductors
MNS Capacitors
Resistors
Multiplier Diodes:
Frequency Multiplication
Waveshaping

## Slide 6: PIN Diodes
Switching
Attenuation Receiver Protector Limiting

## Slide 7: PIN Diodes
PIN Diodes are current-controlled RF resistors
Primarily used in control circuits
  Switches
  Attenuators
  Limiters
MACOM PIN diodes can be made from Si, GaAs or AlGaAs

## Slide 8: PIN Diodes
PIN Diodes used in switches typically have low capacitance and low series resistance
I layer thickness and thermal resistance determine RF power handling
PIN Diodes used in attenuators typically have
  low capacitance for low insertion loss
  thick I layers for large available range of resistance and low distortion
PIN Diodes used in limiters typically have low capacitance for low insertion loss
I layer thickness determines threshold level, recovery time and flat leakage

## Slide 9: PIN Diode Families
Si Discrete | Si HMIC™ | GaAs | AlGaAs
Wide operating frequency range, to 20 GHz Excellent power handling PIN and NIP diodes available I layer: 2 – 300 µm Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Very Wide operating frequency range, to 30 GHz I layer: 8 – 100 µm Available as Single junction devices Multiple junction ICs Wire-bondable or solderable | Wide operating frequency range, to 30 GHz Good power handling Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Extremely Wide operating frequency range, to 100 GHz Lower insertion loss than comparable Si or GaAs switches I layer: 3 µm Available as Multiple junction ICs Wire-bondable

## Slide 10
RF Power and Frequency Performance vs Diode Type
MELF
CW Incident Power (W)
0.1
1.0
10
100
1k
0.01
0.1
AlN in 3mm, 4mm DFN
Die
3KV Ceramic
SURMOUNT
SOD, SOT, Without AlN
Flip Chip, BL
1.0
10
100
F (GHz)
Best Choice for SMT
Best Choice for Wire Bonding

## Slide 11
Si PIN DIODE SWITCH ELEMENT
Series PIN Diode Element
Shunt PIN Diode Element
Series PIN Diode, Thermal-to-Ground Element
Series-Shunt PIN Diode Element
Series, Shunt or Series-Shunt PIN Diodes
SMT Plastic Package
Medium Power Handling

## Slide 12: Discrete Kilovolt PIN Diodes
Features
High Voltage Handling:
  Up to 2000 V, 3000 V
Power Handling: 1 kW
Operate from LF to 500 MHz
Long Carrier Lifetime: 30 µs, 65 µs
Very Low Thermal Resistance:
3 C/W, 4 C/W
Very Low Resistance: 0.1 Ω, 0.15 Ω
Applications
High Power and High Voltage Switching
Plasma Etching Systems
HF Radio Antenna Tuners

## Slide 13: Discrete High Power MELF PIN Diodes
Available in Tape & Reel
Features
High Voltage Handling: Up to 1100 V
200+ W Power Handling
Operate/Tunable from LF to 2.5 GHz
Surface Mountable
Non-Magnetic Versions
Superior Heat Management
Low Series Resistance
Applications
High Power Switches
Attenuators
Magnetic Resonance Imaging (MRI) Receiver Protection
#1 Supplier of MELF PIN Diodes
Notes: February 10, 2017

## Slide 14: Discrete Diodes – Limiters
Limiter diodes can be thought of as RF-voltage-controlled variable attenuators
  When input signal is small,
    limiter diode impedance is high
    RF signal is not attenuated
  When RF signal is large,
    it forces the diode’s impedance to be small
    which reflects the input signal back to its source
  No external control signal is required for the limiter to operate
  DC current return path (RF choke) is required
  Diode I layer thickness determines input power level at which the limiter “turns on”
    Threshold level = input 1 dB compression point

## Slide 15: Discrete Diodes – Limiters
Limiter diodes available
  Die Versions (to 20 GHz)
  Available in Ceramic & Plastic Packages (up to 12 GHz)
  Low Capacitance
  I layers from 2 µm to 40 µm
  Cascadable for Increased Power Handling and Limiting
    Thinnest diode placed at output stage
      Determines threshold level, spike leakage
    Thickest diode placed at input stage
      Determines power handling, recovery time
/4
I standing wave
V standing wave
Thin “clean-up” limiter
Thick “coarse” limiter

## Slide 16
Discrete Limiter Products
Schottky-Limiter-PIN Shunt Antiparallel Pair
Shunt Limiter PIN
Limiter PIN
Broadband Performance to 12 GHz and Higher
Several Packages Available Including
  Low Inductance Shunt Configuration Plastic 1.5 X 1.2 mm DFN
  Ceramic
  Chips
Cascadable

## Slide 17: PIN Switches
Modules Single-Chip

## Slide 18: AlGaAs PIN Diode Switches
SP5T
Product Offering
  SPST to SP8T
Features
  Operating Frequency = 50 MHz - 70 GHz
  Maximum RF Average Incident Power = 0.25 W CW
  AlGaAs ~ 0.3 dB Lower IL (20 GHz) vs. GaAs & Si Switches
  Very Low Insertion Loss
  Excellent Isolation
  Low Switching Time
SPST
SP2T

## Slide 19: AlGaAs SP3T W Band Switch MASW-011029
Broadband Operating Frequency: 60 - 110 GHz
Insertion Loss:1.3 dB Typical
Isolation: 33 dB Typical
Silicon Nitride Passivation
BCB Scratch Protection
Collision Avoidance Radar
Passive Imaging

## Slide 20: Multichip Module High Power Switches
Input power handling to 200 W CW, 1 kW peak
Frequency Range: 20 MHz – 6 GHz in three bands
Symmetric and Asymmetric Designs
SP2T, SP3T, SP4T, SP6T

## Slide 21: T/R Switch-Limiter Module MSWLM2420-242
Features
Frequency Range: 2 – 4 GHz
  T/R switch with passive receiver protection detector/limiter
    Excellent Rx path insertion loss with 2 W CW receiver protector limiter stage
TX input power: 125 W CW, 200 W pk
  Packaged in 5 x 8 mm, low-thermal-resistance surface-mount module package
  Proven performance in the field
Applications
Phased array radar T/R modules
Radio transceiver

## Slide 22: MASW-011036 Ka-Band High Power Terminated AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss <1 dB; High Isolation >38 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
23 dBm power handling in terminated port
Notes: Delete specs table?

## Slide 23: MASW-010646 Ka-Band High Power Reflective AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss: 0.6 dB
High Isolation: 32 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
Notes: Delete specs table?

## Slide 24: X-Band Terminated SPDT Switch MASW-011071
Low Insertion Loss: 1 dB
High Isolation: 38 dB
Integrated Bias Network and Termination Circuit
Greater than 20 W CW Power Handling @ 70 °C
Lead (Pb)-Free 7 x 7 mm 44-lead PQFN Package
Missile Defense, Weather Radar Systems

## Slide 25: HMIC Si PIN Switches: 2 W, DC – 26 GHz
Products
  MASW-001100-11900W (SPST)
  MASW002100-11910W (SPDT)
  MASW-003100-19220W (SP3T)
  MASW-004100-11930W (SP4T)
  MASW-005100-11940W (SP5T)
Features
  Operating Frequency
    50 MHz – 30 GHz
  Series-Shunt Configuration
  High Isolation: >35 dB
  Low Loss: <1.0 dB Insertion Loss
  Switching Time: 50 ns
  Max RF Incident Power:
    >6.0 W CW @ 2 GHz
    2.0 W CW @ 22 GHz
  RoHS Compliant
SP5T
SP3T w/ Integrated Bias Network
Notes: 25

## Slide 26: HMICTM Wire-Bondable Switches
Features
SPST through SP6T
Broadband Performance to 26 GHz
Wire /Ribbon Bond Connections
Available With or Without Integrated Bias Networks
SP3T with Bias Network
SP5T without Bias Network

## Slide 27: HMICTM SP2T High Current MASW-011052
Broad Bandwidth: Specified up to 18 GHz, Usable up to 26 GHz
Integrated Bias Network: High Bias Current +/- 60 mA
Low Insertion Loss/High Isolation
Glass Encapsulation Construction
RoHS Compliant and 260 °C Reflow Compatible

## Slide 28: HMICTM SP3T High Current MASW-011053
Broad Bandwidth: Specified up to 18 GHz, Usable up to 26 GHz
Integrated Bias Network: High Bias Current +/- 60 mA
Low Insertion Loss/High Isolation
Glass Encapsulation Construction
RoHS Compliant and 260 °C Reflow Compatible

## Slide 29: Limiter Modules

## Slide 30: High Power Limiter Modules
Industry-leading input power handling as high as
  300 W CW
  2 kW peak
No external control signal or bias required
Available as
  Single stage
  Dual stage
  Detector/limiter
Available in VHF, UHF, L, S and C bands
Packaged in low-thermal-resistance surface-mount hermetic or nonhermetic module packages

## Slide 31: Tuning Varactor Diodes
VCO Phase Shifter

## Slide 32: Tuning Varactor
Tuning varactors are PN junction diodes which act as voltage-controlled variable capacitors
The depletion region at the junction acts as the dielectric layer of a parallel plate capacitor
  Physically separates the P and the N layers, which act as the plates
Reverse bias voltage magnitude controls the thickness of the dielectric layer, which controls the capacitance of the varactor
p
n
depletion region
d
V
-
+
+++++++++++++++++++++++++++++
- - - - - - - - - -

## Slide 33: Tuning Varactor Diodes
Large Variety of silicon (Si) and gallium arsenide (GaAs) tuning varactors
Available as chips and in a wide variety of packages
Si
  Abrupt junction
  Hyperabrupt junction
GaAs
  Abrupt junction
  Constant Gamma hyperabrupt junction
Chart: Reverse Voltage (V)
| 0.1 | 0.5 | 1 | 1.5 | 2 | 3 | 4 | 5 | 5.5 | 6 | 6.5 | 7 | 7.5 | 8 | 8.5 | 9 | 9.5 | 10
 | 8.86 | 7.2636 | 6.1239 | 5.3971 | 4.8818 | 4.1834 | 3.7207 | 3.3851 | 3.2484 | 3.1273 | 3.0189 | 2.9212 | 2.8326 | 2.7516 | 2.6773 | 2.6087 | 2.5453 | 2.4863
 | 8.86 | 7.2453 | 5.9714 | 5.1212 | 4.5085 | 3.6767 | 3.1325 | 2.7453 | 2.5902 | 2.4541 | 2.3336 | 2.226 | 2.1294 | 2.042 | 1.9625 | 1.8899 | 1.8233 | 1.7619
 | 8.86 | 6.7753 | 5.2355 | 4.2659 | 3.5994 | 2.7424 | 2.215 | 1.8577 | 1.7191 | 1.5997 | 1.4958 | 1.4046 | 1.3239 | 1.252 | 1.1874 | 1.1292 | 1.0764 | 1.0284
 | 8.86 | 6.17 | 4.37 | 2.96 | 1.88 | 0.95 | 0.77 | 0.7 | 0.68 | 0.67 | 0.66 | 0.65 | 0.64 | 0.64
 | 8.86 | 6.3358 | 4.5902 | 3.5535 | 2.8736 | 2.0455 | 1.5662 | 1.2571 | 1.141 | 1.0428 | 0.95885 | 0.88633 | 0.82312 | 0.76759 | 0.71845 | 0.6747 | 0.63553 | 0.60026
 | 8.86 | 5.9248 | 4.0245 | 2.9601 | 2.2942 | 1.5257 | 1.1075 | 0.85067 | 0.75725 | 0.67975 | 0.61463 | 0.55928 | 0.51176 | 0.47062 | 0.4347 | 0.40313 | 0.37521 | 0.35037
Si, GaAs Abrupt
GaAs =0.75
GaAs =1.0
GaAs =1.25
GaAs =1.5
Si Hyperabrupt

## Slide 34: Schottky Diodes
Si and GaAs Frequency Mixing Detection

## Slide 35: GaAs Flip Chip Schottky Diodes
Features
Available As:
  Single Junction
  Series Tees
  Reverse Series Tees
  Antiparallel Pairs
  Unconnected Pairs
Low Series Resistance
Low Junction Capacitance
Applications
Mixer and Detector Applications

## Slide 36: GaAs Beamlead Schottky Diodes
Features
Single Barrier Height
Frequency Range: DC – 40 GHz
Available as
  Single Junction
  2-, 4- and 6-Junction Series Tees
  Antiparallel Pairs
  4-, 8- and 12-Junction Ring Quad
Low Series Resistance
Low Junction Capacitance
Applications
Mixer and Detector Applications

## Slide 37: HMICTM Discrete Schottky Diodes
Features
Surmount Single-Junction Si Schottky diodes
Low, Medium and High Barrier Heights Available
Frequency Range: DC – 30 GHz
Very Low Series Resistance
Very Low Junction Capacitance
Solderable – No Wire Bonds Required
Applications
Mixers and Detectors
Receiver Protector Limiters

## Slide 38: Flip Chip Diodes
PIN
Schottky
Varactor

## Slide 39: Solderable Flip Chip Devices
Parameter | Units | MAVR-000120-1141
Frequency | GHz | Up to 30 GHz
Capacitance @ 0 V | pF | 1.1 pF Typical
Capacitance @ 4 V | pF | 0.30-0.40 pF
Capacitance @ 10 V | pF | 0.14-0.20 pF
Gamma 2-12 V | - | 0.9-1.1
Q | - | 3000 min
Breakdown Voltage | V | 20 V min
Size | mm | 0.75 X 0.40 mm
Parameter | Units | MADS-01317-1500
Frequency | GHz | Up to 80 GHz
Capacitance @ 10 V | pF | 0.045 pF Typical
Series Resistance | - | 4  Typical
Breakdown Voltage | V | 4.5 V min
Size | mm | 0.75 X 0.40 mm
Parameter | Units | MADP-000907-1402
Frequency | GHz | Up to 30 GHz
Capacitance @ 10 V | pF | 0.025 pF Typical
Series Resistance | - | 7  max
Breakdown Voltage | V | 50 V min
Size | mm | 0.67 X 0.35 mm
Ultra Low Capacitance
Millimeter Wave Switching & Cutoff Frequency
Silicon Nitride Passivation
Polyimide Scratch Protection
Cu/Ni/Au Solderable Terminals
RoHS Compliant
PIN Diode - Switching
Schottky Diode – Mixer/Detector
Varactor Diode – VCO/Phase Shifter

## Slide 40: Passive Devices
HMIC™ Bias Networks
Attenuators
MNS Capacitors Spiral Inductors Resistor Networks

## Slide 41: MABT-011000 2-18 GHz HMICTM Surmount Bias Network
HMIC™ Surmount Technology
Broadband Performance 2 – 18 GHz
Parameter | Frequency (GHz) | Target Min | Target Avg | Target Max
Insertion Loss | 2 | - | 0.1 | 0.50
 | 6 |  |  | 
 | 12 |  |  | 
 | 18 |  |  | 
RF – DC Isolation | 2 | 30 | 35 | -
 | 6 |  |  | 
 | 12 |  |  | 
 | 18 |  |  | 
Input Return Loss | 2 | 15 | 17 | -
 | 6 |  |  | 
 | 12 |  |  | 
 | 18 |  |  | 
Output Return Loss | 2 | 15 | 17 | -
 | 6 |  |  | 
 | 12 |  |  | 
 | 18 |  |  | 
High current ±60mA; Voltage ±50V

## Slide 42: Thin Film Passive Products: Capacitors
Products:
  Single Capacitors
  Binary Capacitor Networks
  C = 1 – 500 pF
Features:
  Si3N4 & Si02 Capacitor Dielectrics provide Proven Reliability, Stability and Good Q >30 @ 2 GHz
  Compact Size < 100 mil sq.
Applications:
  Bias networks
  Filters from DC - 40 GHz

## Slide 43: Thin Film Passive Products: Inductors
Products:
Surface Mount Inductors,
L = 5 - 300 nH
Features:
Surface Mount Spiral Inductors on Quartz Substrates
Q > 50 @ 1 GHz.
Applications:
Bias networks

## Slide 44: Thin Film Passive Products: Resistors & Attenuators
Products:
DC – 20 GHz Attenuator Products.
  α = 1 - 30 dB in 1 dB steps
Surface Mount Resistors & Resistor Networks
  R = 1 Ω – 100 kΩ
Features:
TCR of TaN Thin Film Resistors < 100 ppm/º C.
TCR of NiCr Thin Film Resistors < 10 ppm/ºC.
Applications:
RF Power Management
Bias networks

## Slide 45: Thank You

## Slide 46: Appendix

## Slide 47: Discrete Diodes – Si PIN Chips
High Voltage Handling: up to 1000 V
Power Handling: 200+ Watts
Operate from LF to 18 GHz
Chip and Wire Assembly
Low Series Resistance
Applications: Switching and Attenuating
Part Number | Breakdown Voltage (V) | Capacitance (pF) | Series Resistance () | Carrier Lifetime (s) | Thermal Resistance (ºC/W) | I-region (m)
MADP-000165-01340W | 200 | 0.06 | 2.50 | 0.20 | 150 | 19
MA4P161-134 | 100 | 0.10 | 1.50 | 0.150 | 65 | 13
MA47416-132 | 200 | 0.15 | 6.00 | 2.00 | 30.0 | 110
MA47418-134 | 200 | 0.15 | 3.00 | 1.00 | 25.0 | 48
MA4P203-134 | 100 | 0.15 | 1.50 | 0.150 | 75.0 | 13
MA4P303-134 | 200 | 0.15 | 1.50 | 0.20 | 85 | 19
MA4P404-132 | 250 | 0.20 | 0.70 | 0.60 | 30.0 | 28
MA4P504-132 | 500 | 0.20 | 0.60 | 1.00 | 35.0 | 44
MA4P604-131 | 1000 | 0.30 | 1.00 | 3.00 | 10.0 | 96
MA4P505-131 | 500 | 0.35 | 0.45 | 2.00 | 14.0 | 96
MA4P606-131 | 1000 | 0.60 | 0.70 | 4.00 | 8.0 | 96
MA4P506-131 | 500 | 0.70 | 0.30 | 3.00 | 11.0 | 51
MA4P607-212 | 1000 | 1.30 | 0.40 | 5.00 | 4.0 | 125
Notes: February 10, 2017

## Slide 48: Discrete Diodes – Si NIP Chips
High Voltage Handling: up to 500 V
Power Handling: 50+ Watts
Operate from LF to 12+ GHz
Chip and Wire Assembly or Available in Packages
Low Series Resistance
Applications: Switching and Attenuating
Notes: February 10, 2017

## Slide 49: Si Mesa Beamlead PIN Diodes
Rugged Silicon-Glass Construction
Silicon Nitride Passivation
Low Parasitic Capacitance and Inductance

## Slide 50: Si Planar Beamlead PIN Diodes
Rugged Silicon-Glass Construction
Silicon Nitride Passivation
Low Parasitic Capacitance and Inductance

## Slide 51: Flip Chip Products
PIN Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct Max | Rs Typical | Material
 |  | (GHz) | (V) | (pf) | () | 
MA4GP907 | Single | 40 | 45 | 0.025 | 4.2 | GaAs
MA4AGP907 | Single | 50 | 50 | 0.020 | 4.2 | AlGaAs
MA4FCP200 | Single | 40 | 50 | 0.015 | 2.8 | HMIC
MA4FCP300 | Single | 30 | 70 | 0.025 | 2.6 | HMIC
MA4FCP305 | Single | 18 | 40 | 0.050 | 2.1 | HMIC
Varactor Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct 4V | Gamma | Material
 |  | (GHz) | (V) | (pf) |  | 
MA46H146 | Single | 60 | 26 | 0.033-0.06 | 1 | GaAs
MA46H120 | Single | 60 | 15 | 0.20-0.40 | 0.5 | GaAs
Low Capacitance Devices

## Slide 52: Discrete High Power MELF PIN Diodes
Available in Tape & Reel
High Voltage Handling: Up to 1100 V
200+ W Power Handling
Operate/Tunable from DC to 2.5 GHz
Surface Mountable
Non-Magnetic Versions
Superior Heat Management
Low Series Resistance
Applications
High Power Switches
Attenuators
Magnetic Resonance Imaging (MRI)
Part Number | Breakdown Voltage | Total Capacitance | Series Resistance | Carrier Lifetime | Thermal Resistance 
 | (V) | (pF) | () | (s) | (ºC/W)
MA4P504-1072T | 500 | 0.5 | 0.6 | 1.0 | 15
MA4PH236-1072T | 200 | 0.5 | 3.00 | 1.5 | 25
MA4PH238-1072T | 200 | 0.5 | 6.00 | 2.0 | 25
MA4P404-1072T | 250 | 0.6 | 0.60 | 0.6 | 10
MA4P505-1072T | 500 | 0.7 | 0.45 | 2.0 | 6
MA4P7006F-1072T | 600 | 0.7 | 0.90 | 3.0 | 50
MA4P7417-1072T | 800 | 0.7 | 0.80 | 6.5 | 13
MA4P7104F-1072T | 400 | 1.0 | 0.50 | 2.5 | 50
MA4P506-1072T | 500 | 1.0 | 0.30 | 3.0 | 10
MA4P1250-1072T | 50 | 1.2 | 0.75 | 2.0 | 15
MA4PH235-1072T | 35 | 1.2 | 0.50 | 0.3 | 20
MADP-000234-10720T | 500 | 1.7 | 0.25 | 1.5 | 30
MA4P4301F-1091T | 100 | 2.0 | 1.00 | 8.0 | 30
MA4P4306F-1091T | 600 | 2.0 | 1.00 | 8.0 | 30
MA4P4006F-1091T | 600 | 2.2 | 0.50 | 6.0 | 20
MA4P1450-1091T | 50 | 2.5 | 0.75 | 2.0 | 5
MA4P7418-1072T | 1100 | 0.8 | 1.20 | 5.0 | 13
Non Magnetic Package | MA4P7441F-1091T | 100 | 2.2 | 0.50 | 18 | 5
 | MA4P7446F-1091T | 600 | 2.2 | 0.50 | 18 | 6
 | MA4P7452F-1072T | 150 | 0.7 | 0.90 | 9 | 15
 | MA4P7461F-1072T | 100 | 1.0 | 0.50 | 6 | 15
 | MA4P7464F-1072T | 400 | 0.8 | 0.60 | 4.5 | 20
 | MA4P7470F-1072T | 800 | 0.7 | 0.80 | 6.5 | 13
 | MADP-000235-10720T | 35 | 1.2 | 0.50 | 0.3 | 20
#1 Supplier of MELF PIN DIODES
Notes: February 10, 2017

## Slide 53: PIN DIODE SWITCH ELEMENT
Discrete Series PIN Diode
Plastic Package
Medium Power Handling
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MSWSE-005-10S | 5 | 6 | 0.15 | 0.2 | 0.25 | 26 | 17 | 10 | 402
MSWSE-005-15 | 4 | 6 | 0.2 | 0.25 | 0.45 | 24 | 17 | 10 | 503
MSWSE-010-15 | 10 | 2.5 | 0.25 | 0.25 | – | 18 | 9 | – | 503
MSWSE-010-15S | 10 | 3 | 0.05 | 0.25 | – | 20 | 15 | – | 0402P
MSWSE-010-16S | 10 | 3 | 0.06 | 0.08 | – | 20 | 14 | – | 0402P
MSWSE-020-05 | 20 | 1 | 0.05 | – | – | 8 | – | – | 503
MADP-010630-13920T | 25 | 3 | 0.15 | 0.35 | - | 17 | 9 | - | 0805
MSWSE-020-10 | 20 | 1 | 0.03 | – | – | 18 | – | – | 503
MADP-010631-13920T | 40 | 1 | 0.05 | 0.08 | - | 7 | - | - | 0805
MSWSE-040-10 | 40 | 3 | 0.1 | 0.2 | – | 20 | 12 | – | 0805P
MSWSE-044-10 | 40 | 2 | 0.15 | 0.3 | – | 15 | 8 | – | 0805P
MSWSE-050-10 | 50 | 1 | 0.1 | – | – | 10 | – | – | 0805P
MADP-010633-13920T | >50 | 3 | 0.15 | 0.30 | - | 15 | 7 | - | 0805
MSWSE-050-17 | 40 | 3 | 0.06 | 0.1 | – | 18 | 11 | – | 0805P
MSWSER-070-10 | 80 | 0.8 | 0.06 | – | – | 10 | – | – | 3023
MSWSER-100-05 | 80 | 0.8 | 0.15 | – | – | 10 | – | – | 3023
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package*
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MEST2G-010-20 | 10 | 10 | 0.3 | 0.3 | 0.45 | 31 | 23 | 18 | 2012
MEST2G-020-15 | 20 | 6 | 0.2 | 0.22 | 0.3 | 25 | 20 | 11 | 2012
MEST2G-050-45 | 50 | 2.5 | 0.15 | 0.15 | – | 16 | 10 | – | 2615
MEST2G-050-80 | 50 | 1.5 | 0.15 | 0.2 | – | 14 | 8 | – | 2615
MEST2G-010-20 | 10 | 10 | 0.3 | 0.3 | 0.45 | 31 | 23 | 18 | 2012

## Slide 54: PIN DIODE SWITCH ELEMENT
Part Number | Rated CW Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package*
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MEST2G-025-10 | 25 | 4 | 0.06 | 0.3 | - | 18 | 12 | - | CM32
MEST2G-080-25 | 80 | 10 | 0.2 | 0.25 | 0.45 | 30 | 24 | 17 | CM27
MEST2G-100-20-CM33 | 100 | 2.6 | 0.15 | 0.2 | – | 16.5 | 10 | – | CM33
MEST2G-150-10-CM30 | 15W | 1 | 0.07 | - | - | 6 | - | - | CM30
MEST2G-150-10-CM32 | 150 | 2 | 0.12 | 0.16 | - | 12 | 6 | - | CM32
MEST2G-160-10-CM33 | 160 | 2.8 | 0.06 | 0.6 | - | 28 | 20 | - | CM33
MADP-011037 | >125 | 3 | 0.1 | 0.3 | - | 16 | 8 |  | 3mm QFN
Die mounted on thermally-conductive, electrically-insulating substrate
  Very low thermal resistance for high-power handling
CMxx Packages:
QFN Package:

## Slide 55: Shunt PIN Element
Part Number | Rated Power Max (W) | Frequency Maximum (GHz) | Insertion Loss Typical |  |  | Isolation Typical |  |  | Package
 |  |  | Frequency (GHz) |  |  | Frequency (GHz) |  |  | 
 |  |  | 1 | 2.5 | 6 | 1 | 2.5 | 6 | 
MSWSH-020-24 | 25 | 26 | 0.05 | 0.2 | 0.3 | 28 | 27 | 26 | 2020
MSWSH-020-30 | 20 | 6 | 0.05 | 0.15 | 0.35 | 35 | 31 | 26 | 2012
MSHSH-040-30 | 40 | 6 | 0.04 | 0.1 | 0.3 | 35 | 32 | 36 | 2012
MSWSHC-040-40 | 40 | 10 | 0.1 | 0.2 | 0.4 | 35 | 55 | 50 | 2615
MSWSHB-020-30 | 40 | 10 | 0.02 | 0.08 | 0.13 | 40 | 40 | 35 | 2012
Plastic Over-Mold Package
Very Low Inductance Package for High Isolation

## Slide 56: HMICTM Discrete Diode Solution
Part Number | Size (mils) | VB (V) | 1 MHz | 100 MHz |  |  | 1 GHz |  |  |  |  | Lifetime (ns) | Nominal I-region (m)
 |  |  | Cj 40 V (pF) | Rs 10 mA () | Rs 20 mA () | Rs 100 mA () | Cj 40 V (pF) | Rs 10 mA () | Rs 20 mA () | Rs 50 mA () | Rs 70 mA () |  | 
MADP-042305 | 22 X 41 | 80 | 0.13 |  |  |  | 0.14 |  | 1.32 | 1.18 |  | 180 | 7
MADP-042405 | 22 X 41 | 80 | 0.57 |  |  |  | 0.58 |  | 0.62 | 0.58 |  | 255 | 7
MADP-042505 | 22 X 41 | 80 | 0.27 |  |  |  | 0.27 |  | 0.83 | 0.76 |  | 210 | 7
MADP-042905 | 22 X 41 | 80 | 0.06 |  |  |  | 0.06 |  | 3.14 | 2.6 |  | 140 | 7
MA4SPS302 | 23 X 55 | 70 | 0.40 | 1 |  |  | 0.30 | 1.3 |  |  |  | 460 | 10
MA4SPS402 | 20 X 49 | 70 | 0.034 | 4.6 |  |  | 0.04 | 5 |  |  |  | 200 | 10
MADP-017015-1314 | 60 X 30 | 115 | 0.32 |  |  |  | 0.31 | 0.72 |  |  | 0.51 | 1300 | 15
MADP-030015-1314 | 60 X 30 | 115 | 0.79 |  |  |  | 0.78 | 0.49 |  |  | 0.38 | 1600 | 15
MADP-017025-1314 | 60 X 30 | 135 | 0.23 |  |  |  | 0.23 | 1.01 |  |  | 0.64 | 2300 | 25
MADP-030025-1314 | 60 X 30 | 135 | 0.50 |  |  |  | 0.50 | 0.65 |  |  | 0.45 | 2800 | 25
MA4SPS502 | 23 X 57 | 200 | 0.14 |  | 2.4 | 1.4 | 0.09 |  |  |  |  | 2800 | 50
MA4SPS552 | 12 X 22 | 200 | 0.08 |  | 2.4 | 1.7 | 0.06 |  |  |  |  | 2500 | 50
MA4SPS421 | 20 X 41 | 200 | 0.09 |  |  |  | 0.07 | 6.2 |  |  |  | 5000 | 100
MA4SPS422 | 20 X 41 | 200 | 0.18 |  |  |  | 0.13 | 3.1 |  |  |  | 10000 | 100
MADP-042308-1306 | 20 X 41 | 100 | 0.20 |  |  |  | 0.10 |  | 1.38 | 1.18 |  | 280 | 10
MADP-042408-1306 | 20 X 41 | 100 | 0.50 |  |  |  | 0.37 |  | 0.67 | 0.61 |  | 380 | 10
MADP-042508-1306 | 20 X 41 | 100 | 0.30 |  |  |  | 0.18 |  | 0.97 | 0.87 |  | 310 | 10
MADP-042908-1306 | 20 X 41 | 100 | 0.15 |  |  |  | 0.05 |  | 3.63 | 3.02 |  | 230 | 10
Surmount PIN diodes
Available I-region Thickness: 7 to 100 µm

## Slide 57: Discrete Diodes – Limiters
Die Versions (to 20 GHz)
  Available in Ceramic & Plastic Packages (up to 12 GHz)
  Low Capacitance
  Cascadable for Increased Power Handling and Limiting
  Au-doped and non-Au-doped diodes available to optimize recovery time and flat leakage power
Part Number | Min VB | Max VB | Min Cj @ 0 V | Max Cj @ 0 V | Max Rs @ 10 mA | Nominal Characteristics |  |  | 
 |  |  |  |  |  | Carrier Lifetime | Intrinsic Region Thickness | Contact Diameter | Thermal Resistance
 | V | V | pF | pF |  | ns | m | mils | ºC/W
MA4L011-134 | 15 | 35 | 0.08 | 0.18 | 2.10 | 10 | 2 | 1.2 | 175
MA4L021-134 | 20 | 35 | 0.10 | 0.20 | 2.10 | 10 | 2 | 1.2 | 175
MA4L022-134 | 20 | 35 | 0.09 | 0.19 | 2.00 | 10 | 2 | 1.2 | 175
MADL-011009-0134 | 20 | 35 | 0.16 | 0.23 | 1.50 | 10 | 2 | 3.0 | 175
MA4L031-134 | 30 | 50 | 0.14 | 0.21 | 2.00 | 20 | 3 | 1.4 | 150
MA4L032-134 | 30 | 50 | 0.13 | 0.20 | 2.50 | 15 | 3 | 1.5 | 150
MADL-011010-0134 | 30 | 50 | 0.17 | 0.24 | 1.50 | 15 | 3 | 3.0 | 150
MA4L062-134 | 60 | 75 | 0.07 | 0.15 | 2.50 | 10 | 4 | 1.5 | 150
MADL-011011-0134 | 60 | 75 | 0.05 | 0.17 | 2.30 | 10 | 4 | 3.0 | 150
MA4L101-134 | 100 |  |  | 0.15 | 2.00 | 90 | 13 | 3.5 | 30
MADL-000301-0134 | 200 |  |  | 0.20 | 1.50 | 200 | 20 | 3.0 | 30
MA4L401-134 | 250 |  |  | 0.30 | 1.20 | 800 | 25 | 4.5 | 25

## Slide 58: HMIC and AlGaAs MMIC Performance Comparison
Parameter | HMIC | AlGaAs
Products | Switches, Attenuators, Limiters | Switches
Medium | Silicon and Glass | Semi-Insulating GaAs
Die Thickness (um) | 125 | 100
Intrinsic Length (um) | 8 to 100 | 3
I/O Connections | Wire Bondable and SMT | Wire Bondable Only
Passive R,L,C Integration | Yes | Yes
Breakdown Voltage (V) | 50 to 200 | 70
F (GHz) | 0.050 - 30 | 0.050 - 70
Insertion Loss at 10 GHz (SP4T) | 0.6 | 0.45
Switching Speed (ns) | 100 | 15
IIP3 (dBm) | 45 | 25
CW Power Handling, @ 2 GHz (dBm) | +38 | +23

## Slide 59: AlGaAs Products
Topology | Frequency (GHz) | Insertion Loss (dB) | Isolation (dB) | P1dB (dBm) | Reflective or Absorptive | Bias (mA) | Part Number | Package
SPST | 0.05 - 18 18 – 50 | 0.2 0.3 | 22 46 | 23 | Reflective | 10 | MA4AGSW1 | DIE
SPST | 10-50 | 1.2 | 30 | 23 | Absorptive | 10 | MA4AGSW1A | DIE
SP2T | 0.05 - 18 18 – 50 | 0.5 0.7 | 47 33 | 23 | Reflective | 10 | MA4AGSW2 | DIE
SP3T | 0.05 - 18 18 – 50 | 0.6 0.8 | 45 31 | 23 | Reflective | 10 | MA4AGSW3 | DIE
SP4T | 0.05 - 18 18 – 50 | 0.7 1.0 | 41 32 | 23 | Reflective | 10 | MA4AGSW4 | DIE
SP5T | 0.05 - 18 18 – 50 | 1.4 1.9 | 35 30 | 23 | Reflective | 10 | MA4AGSW5 | DIE
SP8T | 0.05 - 18 18 - 50 | 1.5 2.0 | 32 32 | 23 | Reflective | 10 | MA4AGSW8-1 | DIE

## Slide 60: MASW-011036 Ka-Band High Power Terminated AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss <1 dB; High Isolation >38 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
23 dBm power handling in terminated port
Notes: Delete specs table?

## Slide 61: MASW-010646 Ka-Band High Power Reflective AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss: 0.6 dB
High Isolation: 32 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
Notes: Delete specs table?

## Slide 62: HMICTM SP2T 6-14 GHz (Terminated SPDT) MASW-010647
X-Band Terminated SPDT switch
Wire-Bondable Bare Die
Low Insertion Loss/ High Isolation
All Shunt Design; Integrated Bias Network
Glass Encapsulated Construction
Greater than 20 W CW Power Handling @ 85 °C
Silicon Nitride Passivation/Polymer Scratch Protection
RoHS Compliant
Notes: Delete specs table?

## Slide 63: HMICTM Package-less Surface Mountable Si PIN Diode Switches
Topology | Frequency | Insertion Loss (dB) | Isolation (dB) | P0.1dB (dBm) | Part Number
SPDT | 6 GHz 13 GHz 20 GHz | 0.6 0.9 1.2 | 45 31 25 | 36 | MASW-002103-1363
SP3T | 6 GHz 13 GHz 20 GHz | 0.65 0.95 1.25 | 37 28 22 | 36 | MASW-003103-1364
SP4T | 6 GHz 13 GHz 20 GHz | 0.7 1.0 1.3 | 35 30 26 | 36 | MASW-004103-1365
Surface mount - No wirebonds
Packageless - Low parasitics
Series/Shunt multi-throw designs
High Power - 6 W incident

## Slide 64: HMIC™ Si PIN SP2T 6-14 GHz MASW-011021
Specified from 8 GHz to 12 GHz ; Usable 6-14 GHz
Low Insertion Loss / High Isolation
All Shunt Design; Integrated Bias Network
Surface Mountable, Fully Monolithic Die
Glass Encapsulated Construction
20 W Pulsed Power Handling
Silicon Nitride Passivation / Polymer Scratch Protection
RoHS Compliant
Notes: Delete Specs Table?