## Slide 1: MACOM Diode Products – AlGaAs Control Products rev 1
Joe Bukowski, Rick Cory
23 March 2017

## Slide 2
Product Families
Diode Products
PIN/NIP Diodes:
Switching
Attenuation
Limiting
Schottky Diodes:
Detection
Frequency Mixing
Attenuators
Varactor Diodes:
Tuning
Phase Shifting
Passive Devices
RF Chokes/Inductors
MNS Capacitors
Resistors
Multiplier Diodes:
Frequency Multiplication
Waveshaping

## Slide 3
Product Configurations
Discrete Device
HMIC Discrete Surmount
(to 26.5GHz)
Beam Lead/ Flip Chip
(to 70+ GHz)
Plastic
(to 6 GHz)
Integrated Solutions

## Slide 4: AlGaAs PIN Process
PIN Diode Circuits

## Slide 5: PIN Diodes at mmW – the Classic Conundrum
At very high frequencies (>25 GHz) the carrier mobility of Si causes series resistance to increase significantly with increasing frequency
The higher carrier mobility of III-V compound semiconductors makes them preferable at mmW
BUT
We still see junction capacitance and series resistance of PIN structures governed by diode geometry
Junction capacitance must be very small, typically accomplished by reducing the area of the junction
Reduced junction area produces increased series resistance

## Slide 6: Why AlGaAs?
The addition of Al as a p-type dopant in the anode layer of the PIN structure
  Is patented by MACOM
  Increases the bandgap with respect to GaAs
  Creates a barrier to hole “back injection” from the I layer into the P layer
  Enhances forward injection of holes from the P layer to the I layer
  Results in higher charge concentration in I layer under forward bias
Source: Boles, T. et al, AlGaAs mmW PIN Diode Switch: A New Benchmark for Power Handling

## Slide 7: How to Increase Charge in the I Layer?

## Slide 8: Why AlGaAs (cont’d)?
Al dopant
  reduces diode forward-bias series resistance
  has no effect on nonconduction state characteristics
  junction capacitance of AlGaAs junction the same as physically-identical GaAs junction capacitance
Demonstrated a 37% reduction in Rs, and no change in junction capacitance
  Confirmed by fabricated device measurements and simulations
Extends the use of the PIN structure through 100+ GHz
Source: Boles, T. et al, AlGaAs mmW PIN Diode Switch: A New Benchmark for Power Handling

## Slide 9: Rs Reduction & Isolation Validation
Series Loss (dB) vs Freq @ 10mA
Shunt Isolation (dB) vs Freq @ 10mA
Series Isolation (dB) vs Freq @10V
Shunt Loss (dB) vs Freq @ 10V
AlGaAs
GaAs
AlGaAs
GaAs
Source: Boles, T. et al, AlGaAs mmW PIN Diode Switch: A New Benchmark for Power Handling

## Slide 10: Power Handling/Switch Topology
Series Element Switch
  Peak Junction Temperature Dominated by Insertion Loss/I2R Losses
  IL is Direct Function of Device Series Resistance & Incident Power
  Primarily RF Drive Power
  Easily 10%-20% (0.5dB-1.0dB) of Incident Power
  DC Bias Power Very Minor Contributor
  Very Broadband/ISO is Function of Frequency
Shunt Element Switch
  RF Energy Path NOT through Device
  Peak Junction Temperature
    RF Isolation Leakage
    DC Bias Power
    I2R Losses in Metallic Airbridges
    All have Relatively Minor Heating Effect
  Switch IL a Function CJ, NOT Series Resistance
  Multi-Throw Shunt Switch Limitation
    Bandwidth »1 Octave
    l/4 Bias Structures
RF Power Handling
  All Shunt Switch => Highest RF Power Handling
  Essentially NO Intrinsic RF Losses in Active Semiconductors
  Only RF Loss - Metallic Conductors & Capacitive Isolation
Source: Boles, T. et al, AlGaAs mmW PIN Diode Switch: A New Benchmark for Power Handling

## Slide 11: AlGaAs Shunt PIN Diode Structure
MACOM AlGaAs switches are shunt-diode only
Active diode layers are built upon semi-insulating (SI) GaAs substrate
Electrical connection from cathode (n-layer) to backside of wafer is accomplished by through wafer vias (TWVs)
I layer thickness = 3 µm
Nitride
3 mm
Source: Boles, T. et al, AlGaAs mmW PIN Diode Switch: A New Benchmark for Power Handling

## Slide 12: AlGaAs PIN Diode Products
Switching

## Slide 13: PIN Diode Families
Si Discrete | Si HMIC™ | GaAs | AlGaAs
Wide operating frequency range, to 20 GHz Excellent power handling PIN and NIP diodes available I layer: 2 – 300 µm Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Very Wide operating frequency range, to 30 GHz I layer: 8 – 100 µm Available as Single junction devices Multiple junction ICs Wire-bondable or solderable | Wide operating frequency range, to 30 GHz Good power handling Available as: Unpackaged chips SMT packages Ceramic Packages Beam leads | Extremely wide operating frequency range, to 100 GHz Lower insertion loss than comparable Si or GaAs switches I layer: 3 µm Available as Multiple junction ICs Wire-bondable

## Slide 14: PIN Switches
Modules Single-Chip

## Slide 15: AlGaAs Products
Topology | Frequency (GHz) | Insertion Loss (dB) | Isolation (dB) | P1dB (dBm) | Reflective or Absorptive | Bias (mA) | Part Number | Package
SPST | 0.05 - 18 18 – 50 | 0.2 0.3 | 22 46 | 23 | Reflective | 10 | MA4AGSW1 | DIE
SPST | 10-50 | 1.2 | 30 | 23 | Absorptive | 10 | MA4AGSW1A | DIE
SP2T | 0.05 - 18 18 – 50 | 0.5 0.7 | 47 33 | 23 | Reflective | 10 | MA4AGSW2 | DIE
SP3T | 0.05 - 18 18 – 50 | 0.6 0.8 | 45 31 | 23 | Reflective | 10 | MA4AGSW3 | DIE
SP4T | 0.05 - 18 18 – 50 | 0.7 1.0 | 41 32 | 23 | Reflective | 10 | MA4AGSW4 | DIE
SP5T | 0.05 - 18 18 – 50 | 1.4 1.9 | 35 30 | 23 | Reflective | 10 | MA4AGSW5 | DIE
SP8T | 0.05 - 18 18 - 50 | 1.5 2.0 | 32 32 | 23 | Reflective | 10 | MA4AGSW8-1 | DIE

## Slide 16: AlGaAs PIN Diode Switches
SP5T
Product Offering
  SPST to SP8T
Features
  Operating Frequency = 50 MHz - 70 GHz
  Maximum RF Average Incident Power = 0.25 W CW
  AlGaAs ~ 0.3 dB Lower IL (20 GHz) vs. GaAs & Si Switches
  Very Low Insertion Loss
  Excellent Isolation
  Low Switching Time
SPST
SP2T

## Slide 17: AlGaAs SP3T W Band Switch MASW-011029
Broadband Operating Frequency: 60 - 110 GHz
Insertion Loss:1.3 dB Typical
Isolation: 33 dB Typical
Silicon Nitride Passivation
BCB Scratch Protection
Collision Avoidance Radar
Passive Imaging

## Slide 18: MASW-011036 Ka-Band High Power Terminated AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss <1 dB; High Isolation >38 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
23 dBm power handling in terminated port
Notes: Delete specs table?

## Slide 19: MASW-010646 Ka-Band High Power Reflective AlGaAs SPDT PIN Switch
Broadband Performance: 26 to 40 GHz
Low Loss: 0.6 dB
High Isolation: 32 dB
Up to 13 W CW Power, 85 °C
Die with G-S-G RF Pads and DC Bias Pads
Includes DC Blocks and RF Bias Networks
Notes: Delete specs table?

## Slide 20: Thank You

## Slide 21: Appendix

## Slide 22: Flip Chip Products
PIN Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct Max | Rs Typical | Material
 |  | (GHz) | (V) | (pf) | () | 
MA4GP907 | Single | 40 | 45 | 0.025 | 4.2 | GaAs
MA4AGP907 | Single | 50 | 50 | 0.020 | 4.2 | AlGaAs
MA4FCP200 | Single | 40 | 50 | 0.015 | 2.8 | HMIC
MA4FCP300 | Single | 30 | 70 | 0.025 | 2.6 | HMIC
MA4FCP305 | Single | 18 | 40 | 0.050 | 2.1 | HMIC
Varactor Diodes | Configuration | Max Frequency | Breakdown Voltage Vb | Ct 4V | Gamma | Material
 |  | (GHz) | (V) | (pf) |  | 
MA46H146 | Single | 60 | 26 | 0.033-0.06 | 1 | GaAs
MA46H120 | Single | 60 | 15 | 0.20-0.40 | 0.5 | GaAs
Low Capacitance Devices

## Slide 23: HMIC and AlGaAs MMIC Performance Comparison
Parameter | HMIC | AlGaAs
Products | Switches, Attenuators, Limiters | Switches
Medium | Silicon and Glass | Semi-Insulating GaAs
Die Thickness (um) | 125 | 100
Intrinsic Length (um) | 8 to 100 | 3
I/O Connections | Wire Bondable and SMT | Wire Bondable Only
Passive R,L,C Integration | Yes | Yes
Breakdown Voltage (V) | 50 to 200 | 70
F (GHz) | 0.050 - 30 | 0.050 - 70
Insertion Loss at 10 GHz (SP4T) | 0.6 | 0.45
Switching Speed (ns) | 100 | 15
IIP3 (dBm) | 45 | 25
CW Power Handling, @ 2 GHz (dBm) | +38 | +28